Attachment No.: 003

- Cement:

Cement used for the HCB production shall be “Ordinary Portland Cement (OPC) or Portland Pozzolana Cement (PPC)” manufactured by an approved firm and shall comply in all respects with the requirements of ESC D5.201.

“Rapid Hardening Portland Cement (RHPC)” may be used, shall be subject to prior approval by the engineer in order to speed up the progress of the works.

Cement shall be used in the order delivered. It shall be visually checked and tested before being used. Set or partially set cement bags shall be immediately removed from the site.

If required, manufacturers test certificate for each consignment of cement shall be issued with the consignment. Further tests for fineness and compressive strength for consignment already delivered shall be made when required by the engineer.

The quality of the delivered cement to GTZ-IS is tested and guaranteed by the manufacturer. Test certificates are available by manufacturer.

- Water:

Water used for the production of HCB shall confirm to the requirements of ASTM C94.

Water shall be from an approved source and shall be clean, free from oil, acid, alkali, or any vegetable or organic matter harmful to any material with which it is used.

If available drinking water piped supply shall be used.