Hollow Concrete Block

Production & Quality Management

Guidelines

Prepared by Michael Geschke UCBP PM/QM Expert

Content

- Introduction

a    Load bearing walls

b     Non load bearing walls

- Classes of Hollow Concrete Bocks

a    Standard Dimensions

b    Special slab construction block

c    Dimensions used at UCBP

- The HCB production yard

- The Production of Hollow Concrete Blocks

a    Aggregates

b    Water

c    Cement

d    Machinery & Equipment

e    Production process

- Curing and Storage Guidlines

- Operational Staff and Supervision

- Stockpiling

- Keeping records and Reporting

- Introduction

Hollow Concrete Blocks ( HBC ) are blocks manufactured

from concrete and processed into moulds, to achieve the

required physical strength and dimensions to requirements and

standards.

HBC are produced, to construct:

a    Load bearing walls ( Class A & B )

b    Non load bearing walls  ( Class C )

A masonary may be constructed mainly with the following units:

1. Hollow Concrete Blocks

2. Dressed ( natural) stones

3. ( Burnt ) clay bricks

While comparing with others, HCB masonery is a cost and time

efficient and economical solution in construction.

- Classes of Hollow Concrete Blocks

Load bearing HCB             Class A and B

Non load bearing HCB       Class C

a)  Standard Dimensions to ESC.DC.301

10 cm x 20 cm x 40 cm

15 cm x 20 cm x 40 cm

20 cm x 20 cm x 40 cm

b)  For the UCBP the HCB differ from the ESC.

At the UCBP the following HCB will be used:

10 cm x 20 cm x 41 cm

20 cm x 20 cm x 41 cm

20 cm x 22 cm x 54 cm   ripped slab block

- The HCB Production yard

The HCB production area must be even and smooth and should ideal have a power floated surface.

All facilities for production i.e.

Aggregate storage places

Mixing plant

Material storages

HCB storage places

should be as close as possible to the production area.

Attached is a typically layout of a HCB Prefab plant and an engeneers drwg of a HCB production ground floor.

4. The production of Hollow Concrete Blocks

a    Aggregates, i.e. Sand, Gravel, Red Ash:

should be clean, stored separatly close to the mixing plant

All aggregates used for production have to be approved by an

independant concrete labatory!

b    Water: mustbe clean and free of unpurifications

c     Cement: Portland Cement ( OPC ) shall be used as a binder

material for the motar mix.

Cement should be stored in a dry place, moisture free.

d    Machinery & Equipment:

Must be in perfect condition and sufficient in numbers to

suit the daily production needs.

Regular cleaning, maintainence of all machinery & equipment

is essential to keep the agreed quality standards.

An adequate stock of spare parts for all machninery has to be

kept, in order to safe guard production.

e    Production:

Before production can commence, all materials have to be

approved by an official concrete lab.

The mixing and batching will be strictly done on the mix ratio

provided by the official concrete lab.

The mixing ( best results are with a compulsorymixer ) should

be done thouroughly, until a uniform consistence of the

mortar is achieved.

The ready motar mix is poured into the vibrating mould

of the block making machine.

Duration of compaction depends on the type of machine and

vibrator used, but is approx. 3 seconds.

after compaction the unset ( green ) HCB is dropped on the

Floor for curing.

5. Curing Guidlines

Curing is one of the most important activities in the production

process.

The purpose of curing is to replace the evaporating water through sun and / or air.

Also the hydration process, a chemical reaction, needs water to set / harden the mortar.

Once the HCB`s aredropped on the floor, they must be protected from sun and kept constantly moist.

The day after production the HCB are removed from the production floor,placed in two layers on pallets and are again watered till saturation.

The pallets are then covered with waterproof sheets, watered, cured until the seventh day, at least once a day.

After that, put the blocks in five layers on the designated storage place and apply water twice a day.

- Operational Staff andSupervision

In order to achive the best possible quality a specific group of workers should be trained on:

- batching

- mixing

- pouring into the mould

- operating the block making machine

- transporting the blocks

- curing and stocking

If the need of HCB prodution requires shift works, then the precast yard has to belayed out accordantly.

Supervision / Quality control will be carried out by the GC, the concrete lab., the Resident engeneer and the site manager of the implementing agency.

7.    Stockpiling

The GC has to take care that he has always a sufficient stockpile of cement, aggregates and HBC`s on site to buffer delivery problems and to safeguard production on site.

8.   Keeping Records and Reporting

Every daily HCB production has to be marked with the production date, in order to avoid errors in storage/curing time.

The amount of daily production has to be in accordance with the building schedule. The resident engeneer will, on a daily base, record the blocks produced and the quality achieved.

The official concrete lab. will on a monthly base take samples of blocks and aggregates and check those samples in their lab.

Results are to be reported to the resident engeneer and to the site manager of the implementing agency.

The site manager will report on a weekly/monthly turn to the main office of the implementing agency and to the client the progress and the quality of production, based on the resident engeneers reports and own supervision.

| 6.0 Production site of HCB and Pre-cast Beam. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | DESCRIPTION | Unit |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ITEM |  |  | TOTAL | Unit | TOTAL | PREVIOUS MONTH | THIS MONTH | TODATE |
| NO |  |  | QTY. | price | AMOUNT | PLAN | EXEC. | PLANNED | EXECUTED | %com | TOT.PLAN | TOT.EXEC | %com | %COM. | To date plan |
|  |  |  |  |  | (BIRR) | (BIRR) | (BIRR) | Qty | Amount | Qty | Amount | f.plan | Qty | Amount | Qty | Amount | f.plan | f.tot | %of plan from tot. |
| 1 | HCB production |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | HCB conventional type |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 40x20x20 |  | pcs | 823519 | 3.64 | 2997609 | 2997617 | 1373544 | - | - | 4381 | 15947 | - | 823521 | 2997617 | 381728 | 1389491 | 46.4 | 46.4 | 100 |
|  | 40x20x15 |  | pcs | 464674 | 3.00 | 1394022 | 1394022 | 410100 | - | - | - | - | - | 464674 | 1394022 | 136700 | 410100 | 29.4 | 29.4 | 100 |
|  | 40x20x10 |  | pcs | 185052 | 2.14 | 396011 | 396011 | 109898 | - | - | 750 | 1605.00 | - | 185052 | 396011 | 52104 | 111503 | 28.2 | 28.2 | 100 |
|  | Slab HCB (ribbed block) | pcs | 290820 | 3.77 | 1096391 | 1096391 | 420400 | - | - | 1420 | 5353.40 | - | 290820 | 1096391 | 112932 | 425753 | 38.8 | 38.8 | 100 |
|  | u-block |  |  |  | 95655 | 1.70 | 162614 | 162617 | 120356 | - | - | - | - | - | 95657 | 162617 | 70798 | 120356 | 74.0 | 74.0 | 100 |
|  | 16x32 block |  |  | 82523 | 2.00 | 165046 | 165048 | 32960 | - | - | - | - | - | 82524 | 165048 | 16480 | 32960 | 20.0 | 20.0 | 100 |
| Sub-total |  |  | 6211693 | 6211706 | 2467258 |  | 0 |  | 22905 | 0.0 | 1942248 | 6211706 | 770742 | 2490163 | 40.1 | 40.1 |  |
| 2 | **Pre-cast beam** |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 900x120x60mm |  | pcs | 210 | 38.70 | 8127 | 8127 | 9482 | - | - | 25 | 967.50 | - | 210 | 8127 | 270 | 10450 | 128.6 | 128.6 | 100 |
|  | 1500x120x60mm |  | > | 896 | 63.90 | 57254 | 57254 | 47797 | - | - | 51 | 3258.9 | - | 896 | 57254 | 799 | 51056 | 89.2 | 89.2 | 100 |
|  | 3450x120x60mm | > | 1260 | 146.70 | 184842 | 184842 | 188363 | - | - | 177 | 25965.9 | - | 1260 | 184842 | 1461 | 214329 | 116.0 | 116.0 | 100 |
|  | 3960x120x60mm |  | > | 5572 | 167.50 | 933310 | 933310 | 696130 | - | - | 878 | 147065.0 | - | 5572 | 933310 | 5034 | 843195 | 90.3 | 90.3 | 100 |
|  | 4960x120x80mm |  | > | 3438 | 210.60 | 724043 | 724043 | 506282 | - | - | 190 | 40014.0 | - | 3438 | 724043 | 2594 | 546296 | 75.5 | 75.5 | 100 |
|  | 4960x140x80mm |  | > | 288 | 210.60 | 60653 | 60653 | 52860 | - | - | 37 | 7792.2 | - | 288 | 60653 | 288 | 60652 | 100.0 | 100.0 | 100 |
|  | 5000x120x80mm |  | > | 1224 | 211.50 | 258876 | 258876 | 191197 | - | - | 174 | 36801.0 | - | 1224 | 258876 | 1078 | 227998 | 88.1 | 88.1 | 100 |
|  | 5000x140x80mm |  | > | 144 | 211.50 | 30456 | 30456 | 30456 | - | - | - | - | - | 144 | 30456 | 144 | 30456 | 100.0 | 100.0 | 100 |
| sub-total | 13032 |  | 2257561 | 2257561 | 1722567 |  | 0.0 | 1532 | 261864.50 | 0.0 | 13032 | 2257561 | 11668 | 1984432 | 87.9 | 87.9 |  |
| Grand total |  |  | 8469254 | 4515122 | 4189825 |  | 0.0 |  | 284769.74 | 0.0 |  | 8469267 |  | 4474595 | 52.8 | 52.8 |  |  |
| Remark: Key problems: Intermittent failure of production machines, inefficiency in coordinating man power |  |  |  |  |  |  |  |  |  |
|  |  |  |  | and shortage of dia. 6 re.bar. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

| 7.0 QUALITY CONTROL TEST CONDUCTED DURING THE MONTH |
| --- |
| No | Type of material | Tests expected | Date of test | Accepted/Not accepted |
|  |  |  | Ordered |  |
|  | Sand |  |  |  |  |
| 2 | Coarse aggregate |  |  |  |  |
| 3 | Selected material |  |  |  |  |
| 4 | Concrete work |  |  |  |  |
|  | Trial mix |  |  |  |  |
|  | Specimen form |  |  |  |
|  | Foundation footing |  |  |  |  |
|  | Foundation column |  |  |  |
|  | Elevation column |  |  |  |
|  | Beam |  |  |  |
|  | Mat beam |  |  |  |
|  | Grade beam |  |  |  |
|  | Floor beams |  |  |  |
|  | Top tie beams |  |  |  |
|  | Slab |  |  |  |
|  | Ground slab |  |  |  |
|  | Suspended slabs |  |  |  |
| 5 | Hollow blocks |  |  |  |  |
|  | HCB 40x20x20cm |  |  |  |
|  | U - shape blocks |  |  |  |  |
|  | Ribbed slab block |  |  |  |  |
| 6 | Reinforcement bar |  |  |  |
|  | Deformed bar |  |  |  |
|  | Deformed steel |  |  |  |
|  | Wild Steel |  |  |  |
| 7 | Pre-cast beam |  |  |  |  |
| 8 | Others |  | Metal doors | March 31, 2006 | Accepted with remarks |