CHAPTER-6

STANDARD SPECIFICATION OF BUILDING

AND ROAD MATERIALS

6.1 INTRODUCTION

6.1.1Definition

Specification is a written article prepared by technically qualified exports by conducting al lot of research work & certified by a government as an explicit set of requirements to be satisfied by a material, product, system or service

6.1.2 Preparation & Use

Standard technical specification for a country is prepared by considering & studding the following topography, economy climate, Available materials & equipments, development in technology & others. In order to achieve these work a lot of research work, skilled man power, and long period of tie, well organized team devoted for this job much capital, etc. A country may have different towns & cities. Therefore the technical specification should be applicable in these ranges of differences.

Because of all these reasons specified above, many countries in the world especially the developing & underdeveloped countries simply adopt the existing specifications prepared by the developed countries like America (USA), British & others by modifying in some potions satisfy their local requirements or they simply adopt without any modification.

Even if a country have a standard technical specification they don’t simply use for specific project. A pleminary design should be made in order to study the topography, the material available the climatic condition & other different features of that specific area to make   the necessary Amendments on the standard technical specification of the country for that particular project.

The most commonly used standard technical specification in our world now days are ASTM, AASHTO, and BS.

6.1.3)ASTM   (American society of testing and materials)

ASTM international which is organized in 1898 has grown in to one of the largest voluntary standard development systems in the world. ASTM international is a not for profit organization which provides a forum for producers, users, ultimate consumers, & those having a general interest (representatives of Government& Academia) systems, & services

ASTM international published more than 11,300 standards each year. These standards & other related technical information are accepted & used throughout the world. It is the base reference for most of the other standard technical specifications thought the world.

ASTM international standards publish annually containing different volumes on different aspects for example Annual Book of ASTM standards published in 2003 contains 77 Volumes, divided among 16 sections of which construction section contains 13 volumes among the 77.

6.1.4 AASHTO (American Association of state Highway Transport officials)

- AASHTO standard is mainly concerned about Highway standards & basically used ASTM as a reference & It is the most popular & widely used technical specification in road construction & used as a guide in many countries around the world.

It has two parts standard test methods & standard technical specifications, this makes it easier to be used. Since both ASTM & AASHTO are American origin, they are most applicable & most suitable for America’s climate, technology, economy etc. than other countries.

6.1.5 BS (British standard)

As the name implies this standard is prepared in Britain so most suitable in Britain, But many countries in the world especially European those countries colonized by Britain used it as a reference.

Why do specifications of different countries differ?

The difference of technical specification for different country is because of the different in topography. Economy available resources, development in technology, weather condition & other considerations.

i)Economy

The more capital we do have the more we care for people’s safety, comfort & perfection of our work which requires more money to achieve. For example the road which constructed as a highway & upgraded Asphalt in Ethiopia would be of a quality for street roads in a town in America(USA)

ii)Available resources

The available materials in different countries may differ i.e. the material we found in Ethiopia in abundance may not be found in another country or it may be scare resource. The property of the materials may also differ.

iii)Development in technology

Modern equipments treated & artificially prepared suitable materials & computerized working systems may be used which simplifies & increases the perfection of our work.

iv)Weather condition

The effect of the material in hot area is different from cold area for example The amount of asphalt (bitumen) which makes the road sticky in temperate regions may be good (suitable) in tropical region i.e. the property of materials is much dependent of Temperature other weather conditions.

6.1.6 Advantages & disadvantages of using the existing specifications like, ASTM, AASHTO, BS etc.

Advantages

If a country can’t prepare her own technical specification because of the limitation in economy skilled man power & other reasons the ultimate choice is to adopt the existing specification by making the ultimate chaise is to adopt the existing specification by making some amendments to satisfy local requirements & conditions most developing & underdeveloped  countries use this system.

- It sense much amount of many & time

- The number of skilled man power required will be minimized

- Since the specifications are prepared by well organized team who are skilled experienced & devoted for this work, by making a lot of studies & researcher their work is more applicable in other countries too.

- If the development in technology, climatic conditions the available materials of the country almost similar to the country of which the specification is prepared no need of preparing on other technical specification

- These existing specifications have more than 100 years of experience that will help than to pass through the solutions for different problems they faced.

Disadvantage

- It can’t be fully applicable in on other countries

6.1.7 Standard technical specification in Ethiopia

As it is mentioned above in the preparation part preparation of standard technical specification for a country needs much capital skilled experienced man power devoted for this work. But our country Ethiopia has shortage of all these to be capable of preparing her own technical specification. Therefore she simply adopts the existing specifications by doing some modifications to include local considerations. Since country is so much differ in all aspects from the country the specifications are prepared, local consideration will not be enough detailed study should be made during the pleminary design stage for the specific project to use the available materials in the surrounding area, to see the effect of the climatic condition etc. to made the necessary Amendments & modification for the specification for the project. This is a significant problem in Ethiopia for example the read from Awash Melkasa to Soddore show a problem of stickiness, sliding & popping just after the completion of the project. It is because much study was not jade for the area during the design stage this caused not making much amendments & modifications on the specification for that area.

When we come to the standard specification published in Ethiopia Ethiopian road authority(ERA) published technical specification in 1958 by compiling the existing specification (AASHTO,ASTM &BS) adding some modification to include local consideration by 2002 ERA published the modified edition which includes the past experience it is more clarified in the next part. There where also standard technical specification published by Ethiopian Authority for standardization (ESA). Since ERA is concerning about Road construction the specification is also only for road construction. But ESA concerned all for the building & road so now a days in road construction we use standard technical specification of ERA & FOR Building standard technical specification of ESA.

6.1.8 ERA (Ethiopian road Authority)

This standard technical specification is one of the series if “Design manuals, standard contract documents & specification” prepared under a credit financing of the International development agency (IDA) the consulting services were provided by the low’s Berger Group, INC.

This specification has been developed from current international practice appropriately modified to take account of local experience & conditions. It is written for the practicing Engineer.

ERA formed a working Group charged with evaluating & commenting upon the draft manual & guiding the consultant on the preparation of the final manuals. This manual is published & in use starting from 2002.

Appropriate reviews & comments were also provided by agencies & individuals through ERA’S project working Group. The working Group wishes to acknowledge for the contributions made by all other specialists. This specification will be updated & revised from time to time as deemed appropriate.

Since this ERA’S specification is popularly use in our country nowadays we tried to include most of the technical specifications of ERA in this manual, we also tried to include some specifications of ASTM, BS & ASHIO, because ERA’s manual is dependent on these manuals  i.e. it uses them as a reference.

STANDARD SPECIFICATION FOR

BUILDIND MATERIALS

6.2 FINE AGGREGATE (SAND)

- Fine aggregate shall consists of natural sand, manufactured sand or combination of both.

    - Grading requirement

Fine aggregate shall full fill grading requirement given below.

Table 3.1

| Sieve size (mm) | ASTM C-33-02a % pass |
| --- | --- |
| 9.50 | 100 |
| 4.75 (No. 4) | 95-100 |
| 2.36 (No. 8) | 80-100 |
| 1.18 (No. 16) | 50-85 |
| 0.60 (No. 30) | 25-60 |
| 0.30 (No. 50) | 5-30 |
| 0.15 (No. 100) | 0-10 |

Table 3.2

| Sieve size (mm) | BS 812 (% pass) |
| --- | --- |
| 10.00 | 100 |
| 5.00 | 89-100 |
| 2.36 | 60-100 |
| 1.18 | 30-100 |
| 0.60 | 15-100 |
| 0.30 | 5-70 |
| 0.15 | 0-15 |

-  Concrete with fine aggregate grading near the minimum for percent passing the 300µm (No.50) and, 150µm (No. 100) sometimes have difficulties with workability, pumping of excessive bleeding. Thus, the addition of cement or addition of approved mineral admixture to supply the deficient fines.

- The fine aggregate shall have not more than 45% passing any sieve and vertical on the next consecutive sieve of on shown table 3.11 &3.2 2.The fines modules value fine aggregate shall not be less than 2.3 not more than 3.1.

- Fine aggregates shall be free of injurious amount of organic impurities. Except as herein provided, aggregates subjected to the test for organic impurities and producing color darker than the standard shall be rejected.

- Use of the aggregate failing in the test is not prohibited, provided that, when tested for the effect of organic impurities on the strength of mortar, the relative strength at 7 days, calculated in according to test method stated on the method test, is not less than 95%.

- Fine aggregate should have enough soundness value of test from different chemicals, for five cycles of test the soundness test shall have a weighted average not less than 10% when sodium sulfate is used or 15% when magnesium sulfate is used.

6.2.2) General requirement

- Fine aggregate shall full fill the following requirements when tested by the following methods.(Table 3.3)

Table -3.3

| Item No. | Types of test | Method | Allowable limits |
| --- | --- | --- | --- |
| 1 | Organic impurity content | ASTM C 40 | Max plate No. 3 (ASTM C 33) |
| 2 | Silt and clay content a) for concrete subjected to abrasion b) all concrete | ASTM C 117 ” | Max 3% (ASTM C 33) Max 6% (ASTM C 33 |
| 3 | Clay lumps and friable particles | ASTM C 142 | Max 3% (ASTM C 33) |
| 4 | a) soundness test by sodium sulfate b) soundness test by magnesium sulfate | ASTM C 88 ” | Max 3% (ASTM C 33) Max 15% (ASTM C 33) |
| 5 | Finesses modules a) fine sand b) medium sand c) coarse sand |  | 2.20-2.60 2.60-2.90 2.90-3.20 |
| 6 | Chloride content (max) | BS 812 | 600 Mg/litter |
| 7 | Sulfate content | BS 812 | 1000 mg/liter |

6.3 COARSE AGGREGATE

- Coarse aggregate shall consist of gravel, crushed stone. It shall confirm the following grading requirement table below. (see table 3.4) for (ASTM C 33)

6.3.1 General requirement

Coarse aggregate having test results exceeding the limiting value in table- 3.4 given below. It should fulfill the following requirements when tested by the method adopted.

Table -3.4

| Item No. | Types of test | Test method | Allowable limits |
| --- | --- | --- | --- |
| 1 | Coal and lignite content | ASTM C 142 | 1% (ASTM C 33) |
| 2 | Clay limps and fibber particles content | ASTM C 142 | 1% (ASTM C 33) |
| 3 | Dust content | ASTM C 117 | 1% (ASTM C 33) |
| 4 | a) soundness test by Sodium sulfate (Na2 so4) b) soundness test by Magnesium sulfate (Mg so4) | ASTM C 117 ASTM C 117 | Max 12% (ASTM C 33 Max 12% (ASTM C 33 |
| 5 | Los Angeles abrasion (%) wear |  |  |
|  | a) For aggregate to be used in concrete for wear surfaces b) For aggregate to be used in all other concrete work | ASTM 131 ” | Max 30 (ASTM C 33) Max 50 (ASTM C 33) |
| 6 | Aggregate crushing value |  |  |
|  | a) for concrete subjected two wearing surfaces b) for other concrete | BS 812 ” | Max 30% Max 45% |
| 7 | Flakiness index | BS 812 | Max 30% (BS 812) |
| 8 | Aggregate impact value A. for concrete subjected two wearing surfaces B. for other concrete | BS 812 BS 812 | Max 30 % Max 45 % |
| 9 | Chloride content (max) | BS 812 | 600 mg/lit (BS 812) |
| 10 | Sulfate content | BS 812 | 600 mg/lit (BS 812) |

| Sieve Size (mm) | Grading requirement for coarse aggregate (BS 882) |
| --- | --- |
|  | Percentage by mass passing BS sieves for normal size |
|  | Graded aggregates | Single sized aggregate |
|  | 40mm to 5mm | 20mm to 5mm | 14mm to 5mm | 40mm | 20mm | 14mm | 10mm | 5mm |
| 50 | 100 | - | - | 100 | - | - | - | - |
| 37.5 | 90-100 | 100 | - | 85-100 | 100 | - | - | - |
| 20 | 35-70 | 90-100 | 100 | 0-25 | 85-100 | 100 | - | - |
| 14 | 25-55 | 40-80 | 90-100 | - | 0-70 | 85-100 | 100 | - |
| 10 | 10-40 | 30-60 | 50-85 | 0-5 | 0-25 | 0-50 | 85-100 | 100 |
| 5 | 0-5 | 0-10 | 0-10 | - | 0-5 | 0-10 | 0-25 | 45-100 |
| 2.36 | - | - | - | - | - | - | 0-5 | 0-30 |

Table:-3.5 Grading requirement for coarse aggregate

    - Specific gravities

- Specific gravity of cause aggregate is the ratio of density of saturated surface dry of the aggregate to the distilled water at a stated temperature.

- In the computation of quality for concrete mixes, it is the specific gravity of saturated surface dry aggregates that always used. The specific gravities of few types of rocks are given below.

Table:-3.6

| Rock group | Bulk specific gravity |
| --- | --- |
|  | Average | Range |
| Basalt | 2.75 | 2.70 - 2.90 |
| Granite | 2.65 | 2.60 – 2.70 |
| Limestone | 2.65 | 2.60 – 2.70 |
| Sand stone | 2.50 | 2.0 – 2.60 |

6.3.3Water absorption

- The absorption capacity is measure of the porosity of an aggregate. Approximate values of absorption capacity of some types of aggregate are given below.

Table:-3.7

| Material | Absorption capacity % by wt. |
| --- | --- |
| Band | 0-2 |
| Gravel | 0.5 – 1 |
| Basalt | 0 – 0.5 |
| Granite | 0 – 0.5 |
| Limestone | 0.5 – 1 |
| Sand stone | 2 - 7 |

6.3.4 Unit weight

- The unit weight /bulk density/ of aggregate is the mass per unit volume in aggregate.

- The unit weight of aggregate is important for calculating proportion of a concrete mix (especially loose unit weight) general range unit weight of some natural aggregates are indicated below.

Table:-3.8

| Material | Unit weight (kg/m3) |
| --- | --- |
| Sand (dry) | 1320 – 1680 |
| Gravel | 1280 – 1440 |
| Crushed stone | 1250 - 1460 |

6.4 LIGHT WEIGHT AGGREGATE FOR STRUCTURAL

CONCRETE

- This specification covers light weight aggregates intend for use in structural concrete in which the prime consideration is reducing the density while maintaining compressive strength of concrete.

- Two general types of light weight aggregate are covered by this specification, as follows.

- Aggregates prepared by expanding, palletizing or sintering products such as blast furnace slag, clay, diatomite, fly ash, shale, or slate and

- Aggregate prepared by processing natural materials, such as, pumice, scoria or tuff.

- The amount of clay lumps shall not exceed 2% by dry weight.

- The grading shall conform to the requirements as shown below.

Table:-6, Grading requirements for light weight aggregate for structural concrete

| Size designation | Percentage (mass) passing sieves having square opening |
| --- | --- |
|  | 25mm | 19mm | 12.5mm | 9.5mm | 4.75mm | 2.36mm | 1.18mm | 300µm | 150µm |
| Fine aggregate 4.75 mm to 0 | - | - | - | 100 | 85 - 100 | - | 40 - 80 | 10 – 35 | 5 - 25 |
| Coarse aggregate 25.0 to 4.75 mm 19.0 to 4.75 mm 12.5 to 4.75 mm 9.5 to 2.36mm |  |  |  |  |  |  |  |  |  |
|  | 95 – 100 | - | 25 – 60 | - | 0 – 10 | - | - | - | - |
|  | 100 | 90 – 100 | - | 10 – 50 | 0 – 15 | - | - | - | - |
|  | - | 100 | 90 – 100 | 40 – 80 | 0 – 20 | 0 – 10 | - | - | - |
|  | - | - | 100 | 80 – 100 | 5 – 40 | 0 – 20 | 0 – 10 | - | - |
| Combined fire and coarse aggregate. 12.5 mm to 0 9.5 mm to 0 |  |  |  |  |  |  |  |  |  |
|  | - | 100 | 95 – 100 | - | 50 – 80 | - | - | 5 – 20 | 2 – 15 |
|  | - | - | 100 | 90 – 100 | 65 – 90 | 35 – 65 | - | 10 – 25 | 5 - 15 |

- Uniformity of grading: - To assure reasonable uniformity in the grading of successive shipments of lightweight of aggregate in any specimen differs by more than 7% from that of the sample submitted for acceptance tests, the aggregate sample shall be rejected.

- Bulk density /loose/ - the bulk density (loose) of the lightweight aggregates shall conform to the requirements shown below.

Table: - bulk density /loose/ requirements of lightweight aggregate for structured concrete

| Size designation | Maximum dry loose/ bulk density (kg/m3) |
| --- | --- |
| Fine aggregate | 1120 |
| Coarse aggregate | 880 |
| Combined fine and coarse aggregate | 1040 |

6.5) Standard specification for Portland cement.

1)Scope

  - This specification covers eight type of Portland cement as follows

    - Type I for use when the special properties specified for any other type are not required.

    - Type IA air entraining cement for the same uses as type I, where air entrained is desired.

    - Type II for general use more especially when moderate heat of hydration is desired.

    - Type II A – air entrance cement for the same uses as type II, where air entrainment is required.

    - Type III – for use when high early strength is required.

    - Type III A – air entrained cement for the same use as type III, where air entrainment is required.

    - Type IV – for use when low heat of hydration is required.

    - Type V for use when high sulfate resistance is required.

2) Definitions,

    - Portland cement:- a hydraulic cement produced by pulverizing clinker consisting essentially of hydraulic calcium silicates, usually containing one or more of the forms of calcium silicates, usually containing one or more of the forms of calcium sulfate as an inter ground addition.

    - Air entrained Portland cement:- a hydraulic cement produced by pulverizing clinker consisting essentially of hydraulic calcium silicates, usually containing one or more of the forms of calcium sulfate as an inter ground addition and with which there has been inter ground an air entraining addition.

    - Hydraulic cement: - a cement that sets and hardens by chemical interaction with water and is capable of doing so under water.

3) Physical properties

- Portland cement of each type shown above shall conform to the respective standard physical requirements prescribed in table bellow.

Table 1, standard physical requirements

| Cement type | I | IA | II | IIA | III | IIIA | IV | V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Air content of mortar volume % |
| Max | 12 | 22 | 12 | 22 | 12 | 22 | 12 | 12 |
| Min | - | 16 | - | 16 | - | 16 | - | - |
| Fineness, specific surface, m2/kg |
| Air permeability test |
| Average value, min | 280 | 280 | 280 | 280 | - | - | 280 | 280 |
| Min value, anyone sample | 260 | 260 | 260 | 260 | - | - | 260 | 260 |
| Average value, max | 400 | 400 | 400 | 400 | - | - | 400 | 400 |
| Max, value any one sample | 420 | 420 | 420 | 420 | - | - | 420 | 420 |
| Auto clave expansion, max% | 0.80 | 0.80 | 0.80 | 0.80 | 0.80 | 0.80 | 0.80 | 0.80 |
| Compressive strength in Mpa |
| 1 day | - | - | - | - | 12 | 10 | - | - |
| 3 day | 12 | 10 | 10 | 8 | 24 | 19 | - | 8 |
| 7 day | 19 | 16 | 17 | 14 | - | - | 7 | 15 |
| 28 day | - | - | - | - | - | - | 17 | 21 |
| Time of setting using Vicat test apparatus |
| Time of setting in minute, not less than | 45 | 45 | 45 | 45 | 45 | 45 | 45 | 45 |
| Time of setting in minute not more than | 375 | 375 | 375 | 375 | 375 | 375 | 375 | 375 |

6.6 Hollow concrete Blocks

3.6.1) Classification:-

Hollow concrete blocks shall be classified in the following three classes

- Class A and B are load beading units and suitable for:

- External walls pointed, rendered and plastered

- The inner leaf of cavity walls or stonemasonry

- internal walls or partitions

- Panels in steel framed and reinforced steel framed buildings.

- Class C - non- load bearing units suitable for:'

- Non load bearing walls and partitions

- None load beating internal panels in steel framed and reinforced concrete buildings.

Note: Six full size samples shall be tacky from a lot of 4000 blocks or factory threw of hollow concrete blocks are medicates below

3.6.2) Dimensions

- The nominal dimensions of hollow concrete blocks are medicated below

| Breadth (b) (mm) | Height (h) (mm) | Length(L) | Face shel (d)(mm) | Web(e) (mm) | Maximum unit weight(Kg/m3 |
| --- | --- | --- | --- | --- | --- |
| 100 150 200 250 300 | 200 200 200 200 200 | 400 400 400 400 400 | 20 25 30 35 40 | 20 25 25 30 30 | 1200 1200 1200 1200 1200 |

6.6.3) Minimum Compressive Strength

The minimum compressive strength for HCB recording to ESC D3 301 is indicated below

| Class | Average of six Units | Individual Units |
| --- | --- | --- |
|  | Mpa | Kg/cm2 | Mpa | Kg/cm2 |
| A B C | 4.2 3.5 2.0 | 4.2 3.5 2.0 | 3.8 3.2 1.8 | 3.8 3.2 1.8 |

6.7) Sold CLAY BRICKS

Bricks are prismatic units available in a variety of sizes, shapes, textures and colors,

Bricks are manufactured from clay, shale or similar naturally occurring earthy substances and subjected to a heat treatment at cleaved temperature (firing)

6.7.1) Classificatory (According to Ethiopian Code)

- Bricks shall be classified recording to numerical value of their compressive strength, water absorption, saturator coefficient and efflorescence as indicated below (ESC.D4.001)

| Class | Minimum compressive strength | Maximum water absorption % | Maximum saturation coefficient | Maximum unit weight (Kg/m3) |
| --- | --- | --- | --- | --- |
|  | Average of five bricks | Individual brick | Average of five bricks | Individual bricks | Average of five bricks | Individual bricks |  |
|  | MPa | Kg/cm2 | Mpa | Kg/cm2 |  |  |  |  |  |
| A B C D | 20 15 10 7.5 | 200 150 100 75 | 17.5 17.5 7.5 5.0 | 175 125 75 50 | 21 22 No limit No limit | 23 24 No limit No limit | 0.96 0.96 No limit No limit | 0.99 0.99 No limit No limit | 2200 |

6.7.2) Grades of solid brick (According to AASTHO)

Grades of brick are classified in according to their resistance to damage by freezing when wet. Three grades are covered and the grade requirement are shown in table 1

a) Grade SW ( Severe Weathering)   Brick intended for use where  high and uniform Resistance to damage caused by cyclic freezing is desired and where the brick may be frozen when saturated with water.

b) Grade MW (Moderate weathering)   brick intended for use where moderate resistance to cyclic freezing damage is permissible or where the brick may be damp but not saturated with water when freezing occurs.

C) Grade NW (Negligible weathering) Brick with little resistance to cyclic freezing damage but which are acceptable for applications protected from water absorption and freezing.

6.7.3)Physical properties

Appearance - If brick are required to have a particular color, texture, finish uniformity, or limits on crakes, war page or other imperfections detract acting from the appearance they are pureed.

Durability- when Grade is not specified, the requirements for  grade SW shall govern. unless other wise specified by the purchase brick of grade SW shall be accepted

| Designation | minimum compressive strength (Mpa) | Maximum Water | Maximum saturation coefficient |
| --- | --- | --- | --- |
|  | Average of five bricks | Individual | Average of five bricks | Individual | Average of five bricks | Individual |
| Grade SW Grade SW Grade SW | 20.7 17.20 10.3 | 17.20 15.20 8.6 | 17.00 22.00 No limit | 17.00 22.00 No limit | 0.78 0.88 No limit | 0.80 0.90 No limit |

- The use of grade MW brick in wall area above grade is structurally adequate in the severe weathering region, but Grade SW would provide a higher and more uniform degree of resistance to frost action. The degree of durability called for by Grade SW is not necessary for use in wall areas above grade in the moderate weathering reader in the non weathering region, where the average compressive strength of the units is at least 17.2 Mpa.

6.7.4. HOLLOW CLAY Bricks

Hollow clay bricks shall mean a brick with parallel holes passing through it and having an area not less than 25 % of Crosse tonal area.

The nominal dimensions of hollow clay bricks are indicated below

| Nominal dimension(mm) |
| --- |
| Height (h)(mm) | Breadth (mm) | Length (mm) |
| 140 140 160 160 | 250 400 250 400 | 250 250 250 250 |

6.7.5 Form and surface

- The following maximum permissible deviation shall be accepted

a) Plainness not exceeding  4.80mm for a length of 300mm

b) square ness not exceeding 4.80mm for length of 300mm

c) cracks not exceeding 1mm in width.

6.7.6   Compressive strength

- The minimum value of compressive strength of hollow clay bricks shall be as indicated below (Esc. D4, 026)

| Type |  |
| --- | --- |
|  | Average of 5 bricks | Individual bricks |
|  | Mpa | Kg/cm2 | MPa | Kg/cm2 |
| kk,ss,sk | 7 | 70 | 5.5 | 55 |

Note:- KK- With two faces fixed for plastering

SS= With two faces smooth

Sk = With one faces smooth end the other face smooth

6.8) Terrazzo Tiles

Terrazzo tiles shall mean tiles whose wearing  surface is composed of stone chip mixed  with sand, ordinary or colored Portland cement and mechanically ground and filled.

6.8.1) Shape and dimension

The nominal dimension and tolerances of terrazzo tiles shall be as specified below (ESC D/3.303)

| Thickness | Breadth X Length |
| --- | --- |
| Nominal (mm) | Tolerance (mm) | Nominal(mm) | Tolerance (mm) |
| 20 25 30 35 | + 0.30 + 0.30 + 0.30 + 0.30 | 200X200 250X250 300X300 400X400 | + 0.80 + 0.80 + 0.80 + 0.80 |

6.8.2) Water absorption and transverse strength

The water absorption  of individual tiles shall not exceed 8 % when tested age of 28 day. The transverse strength when tested for dry and wet condition 28 days shall have no individual result less than 3 Mpa for dry test and 2 Mpa for wet test.

6.9) CONCRETE

- Concrete is a composite material consisting essentially of a binding medium within which, are embedded particles of a relatively inert filler materials

-In concrete, the binder is cement and the filler material is Aggregate of graded size from sand to process of stone varying document  & shaper .

6.9.1 Properties of fresh concrete.

As soon as H20 is brought in contact with other ingredients of concrete freshly mixed concrete gradually undergoes change until it becomes hold in this plastic state the most important properties are

- Workability

- Consistency

- Segregation

- Bleeding

Workability: - Freshly mixed concrete should be easily to be transported, placed, consolidated and finished without any 	segregate

-The workability of concrete is affected by water content size 			of aggregate, shape of aggregate & grading of aggregate

Consistency: - It is closely related to workability. It is fresh concern 				flows and it indicates the degree of wetness.

Measurement of Workability

Among various method of determine the workability of concrete the most commonly method is slump test

No       Type of construction                               	            slump (cm)

max.           min

  - Heavy mass construction        		        50    	      25

  - Pavements                 			        50  	      25

  - Uninformed footing, casinos & sub. struck    75                25

  - Bridge deck        				         75               25

  - Rein forced foundation wall & footing           100               50

  - Reinforced beams, globs, Wally     	        125              75

  - Columns      				        125              75

6.9.2) Properties of hardened concrete

- In hardened state  the various properties which need consideration ere strength, permeability, Durability, Elasticity, shrinkage & creep

- Strength of concrete is the most important property as far as the structural design is concerned.

- Strength of concrete is measured either in concussive strength of or tensile strength.

- The usual method of compressive strength determination is done on either cubes or cylinder specimen.

- The cylindrical compressive strength is 80 % of cube strength

- Cylindrical or cubical specimens may be used with conversion factors determined from compressive series of tests.

| Size of type of test specimen | conversion factor |
| --- | --- |
| Cubes | 1.05 |
| Cylinder | 1.25 |

- Tangible strength of concrete has low tangible strength, which verges from 8% to 12 % of its compressive strength. An average value of 10 % is generally accepted.

6.9.3) Classes of concrete

- A concrete is graded interims of characteristics compulsive cube strength attained it the   of 28 days in Mpa. The Permissible grades for the two classes of concrete work are giver below

| Class | permissible grades |
| --- | --- |
| I | C 5 C15 C20 C 25 C 30 C 40 C 50 C 60 |
| II | C C C 15 C 20 |

Class I: - concrete works carried out under the directory of super visors r	gestured by the ministry as associate Engineers or above

Class II: - Concrete works claimed out under the direction of supervise 	registered by ministry of by Engineering Aids

| Class | minimum compressive strength (Mpa) | minimum compressive (psi) |
| --- | --- | --- |
| A C y | 28 18 18 | 4000 2500 4000 |

6.9.4) Characteristics compulsive strength

Compressive strength of concrete is determined from test on 156 cube at the age of 28 days.

fc 28 =3/2 *fc7    where – fc28 - the strength of concrete at 28 days

fc7 - the strength of concrete at 7 days

- The characteristics  compressive strength is detained as that strength below which 5 % of all possible strength measure may be expected to fall. In practice concrete may be regarded  has complying with the grade specified for the design

6.9.5 Measures to be tacky in case of non compliance

- the position of concrete which does not full fill the compliance criteria shall be identified

- the structural safety of durability shall be checked by approach   calculations.

- If such structural safety or durability is not issued, the strength of cone rate shall be examined by taking drilled or concrete lamer test is performed.

- If the results of cheek test by non - destructive methods show that the quality of concrete is inadequate or show other defects, the engineer may require alluding test.

- If structural safety and viability are not assured, they the concrete shall be rejected and the structure or member demolished or given & reduced structural grading by limiting service rating.

6.9.6   Standard /Normal mixes of concrete/

-Those are standard mixes which are rich in cement /ordinary Portland cement, and are interred for use where the cost of trial mixes or of cubes testing is not justified.

| concrete Grade | Nominal maxi. size | 40 | 20 | 14 | 10 |
| --- | --- | --- | --- | --- | --- |
|  | workability | medium | High | medium | High | medium | High | medium | High |
|  | Limits of slump test | 30-60 | 60-120 | 20-50 | 50-100 | 10-30 | 30-60 | 10-25 | 25-50 |
| C5 | Total Agg.(Kg) Fine Agg. Volume of concrete (m3) | 640 30-45 0.312 | 550 30-45 0.275 | 540 35-50 0.277 | 480 35.50 0.252 | - - - | - - | - - - | - - - |  |
| C15 | Total Agg.(Kg) Fine Agg. Volume of concrete (m3) | 370 30-45 0.2 | 330 30-45 0.183 | 320 35-50 0.178 | 280 35-50 0.16 | - - - | - - | - - - | - - - |
| C20 | Total Agg.(Kg) Fine Agg. Volume of concrete (m3) | 305 30-35 0.165 | 270 30-40 0.155 | 280 30-40 0.156 | 250 35-45 0.143 | 255 35-45 0.13 | 240 40-50 0.13 | 240 40-50 0.137 | 200 45-50 0.121 |
| C29 | Total Agg.(Kg) Fine Agg. Volume of concrete (m3) | 265 30-35 0.147 | 240 30-40 0.137 | 240 35-40 0.137 | 215 35-45 0.127 | 220 35-45 0.13 | 195 40-50 0.118 | 210 40-50 0.124 | 175 45-5 0.11 |
| C.30 | Total Agg.(Kg) Fine Agg. Volume of concrete (m3) | 235 30-35 0.134 | 215 30-40 0.127 | 210 30-40 0.127 | 190 35-45 0.115 | 195 35-45 0.115 | 170 40-50 0.106 | 180 40-50 0.109 | 150 45-55 0.097 |

6.9.7) Specification of concrete.

1.1 Methods of specifying concrete

- Designed mixes:- their required compressive strength is specified, together with   buy other limits that may be  required, such as maximum aggregates size, minimum cement content, and workability

- Prescribed mixes: - the design resumes responsibility  for designing the mix and stipulates to the producer the mix properties and the materials which shall be employed.

- Standard mixes:- The mix propitious which are appropriate for grades C -          5 to C -30 may be taken see for 9-8

1.2 Constituent Material of concrete

- climate:- The cement used shall be  Portland or Portland puzzling cement with the requirements  of the latest Ethi. Standards requiems of such cements.

- Aggregates: In general aggregates shall comply with the requiems of latest Ethiopian standard for aggregates

- Water :- Mixing water shall be clean and free from harmful matter

|  | Reinforced concrete | plain concrete |
| --- | --- | --- |
| Mild:-Completely protected against whether or aggressive condition | Nominal max-size of Agree |  | Nominal max size | W/C |
|  | 40 | 30 | 20 | 10 |  | 40 | 30 | 20 | 10 |  |
|  | 230 | 260 | 280 | 300 | 0.65 | 220 | 230 | 260 | 280 | 0.70 |
| Moderate: sheltered from seruerrain Buried concrete and concrete continues under water | 270 | 300 | 330 | 350 | 0.55 | 230 | 260 | 290 | 310 | 0.60 |
| Sever :- Exposed to sea water Driving main alternate wetting and drying Subject to heavy condensate or corrosive fumiest | 330 | 370 | 400 | 420 | 0.45 | 280 | 320 | 340 | 370 | 0.50 |

II) STANDARD SPECIFICATION

FOR ROADS

# 6.10 )  Standard specification for sub-bases

(ERA 2000)

6.10.1   Material sources for sub-base

The materials used for the construction of sub base layers shall be either.

- Natural Gravel

- Scoria

- Gravel

- Weathered Rock

- Crushed Grovel

- Crushed rock as clashed Boulders

- Recycled pavement Material

Any other granular material complying with the requirements of this clause.

Material requirements for gravel sub- base

A/ Grading limits

The sub-base material shall comply with one of the parings shown in table below as described in the contract. The material shall have a smooth continuous grading within the limits for grading A, B or c given below.

| Sieve size (mm) | Mass percent passing |
| --- | --- |
|  | A | B | C | D |
| 63.0 | 100 | - | - | - |
| 50.0 | 90-100 | 100 | 100 | - |
| 37.5 |  |  | 80-100 |  |
| 25.0 | 51-80 | 55-85 |  | 100 |
| 20 |  |  | 60-100 |  |
| 9.5 |  | 40-70 |  | 51-85 |
| 5 |  |  | 30-100 |  |
| 4.75 | 35-70 | 30-60 |  | 35-65 |
| 2.0 |  | 20-51 |  | 25-51 |
| 1.18 |  |  | 17-75 |  |
| 0.425 |  | 10-30 |  | 15-30 |
| 0.3 |  |  | 9-50 |  |
| 0.075 | 5-15 | 5-15 | 5-25 | 5-15 |

The complete sub-base shall contain no material having a maximum dimension exceeding 2/3 of the compacted layer thickness.

Sub-base material shall, unless & otherwise authorized, confound to the following requirements when finally placed:

# B/ Grading modulus

The minimum grading modulus shall be 1.5 except where a material, having a lower grading modulus but not less than 1.2, is approved for use by the engineer.

##### C/ Plasticity index

All sub=base materials shall have a maximum plasticity index of 6-12, as described in the contact, & when determined in accordance with AASHTO T-90.The plasticity product (PP=PI X percentage passing the 0.075 mm sieve) shall not be greater than 75.

D/ California Bearing Ratio (CBR)

- The minimum soaked California Bearing. Ration (CBR) Shall be 30% at maximum dry density (MDD)95%

# E/ Compaction Requirements

- The minimum in-situ dry density of sub-base material shall be as specified hereinafter for the layers in terms of a percentage of modified AASHTO density.

I/   95% or 97% as required for material not chemically stabilized.

II/   95% or 96% as required for chemically stabilized material.

# F/ Los Angeles Abrasion

The Los Angeles abrasion value shall not exceed 51% when determined in accordance with the requirements of AASHTO T-96.

#### 3.6.2 Material Requirements for crushed stone sub-base

## General:-

The aggregate used for crushed stone sub-base shall be derived from a parent rock that is hard, Sound, durable, & unlettered. It shall be obtained from sound lock from an approved quall as clear sound boldness. It shall contain no deleterious material such as decomposed rock, clay, shall, or mica .The or shed aggregate shall comply with the following requirements

A/ Grading limits

| Sieve size (mm) | Percentage passing by weight |
| --- | --- |
|  | A | B | C |
| 50.0 | 100 | - | - |
| 37.5 | 95-100 | 100 | - |
| 28 | - | - | 100 |
| 20 | 60-80 | 70-85 | 90-100 |
| 10 | 40-60 | 50-65 | 60-75 |
| 5 | 25-40 | 35-55 | 40-60 |
| 2.36 | 15-30 | 25-40 | 30-60 |
| 0.425 | 7-19 | 12-24 | 13-27 |
| 0.075 | 5-12 | 5-12 | 5-12 |

One of the grading specified (A, B or C) will be used as described in the contract, as as approved as directed by the engineer.

# B/ Grading Modulus

The minimum grading modulus shall be 1.5 except where a material, having a lower grading modulus but not less than 1.2 is approved for use by the engineer

C/ Plasticity index (PI)

- The plasticity index shall not exceed 6.

# D/ Los Angeles abrasion

The Los Angeles abrasion value shall not exceed 54% when determined in accordance with the requirements of AASHTOT-96

# E/ Compaction Requirements

The minimum dry density to which the material shall be compacted shall be 95% unless specified otherwise, shown on the drawings as ordered by the engineer, of the maximum dry density as determined by AASHTP T180. Field dry densities shall be determined by the sand replacement method as specified in AASHTO T 191 as nuclear methods as specified in AASHTO T 238.

# F/ Particle shape; Flakiness index

The flakiness index, determined by testing in accordance with BS 812, part 104 as ASTM D 3398, shall not exceed 35%.

# 6.11  Road Bases

# Scope:-

This division covers the specifications of materials for, & the construction of load base pavement layers from approved base materials. It includes the use of crushed screened or crushed & screened stones as gravels, natural gravels, & stabilized base materials.

6.11.1) Road base material types

The material used for the construction of load base layers shall be one of the following as described in the contract:

- Crushed Rock or stone;

- Naturally occurring Granules Materials, Boulders, Weathered Rock:

- Dense bitumen Macadam.

6.11.2) Material requirements for crushed rock or stone

This material is produced by crushing flesh, quarried rock (GB1) . The material shall be clean & free from organic matter, lumps of clay or other deleterious substances.

A) Grading

The combined grading of the material shall be a smooth continuous curve falling within the grading limits shown in table below 2500/1 when determined in accordance with the requirements of AASHTO T-27. The mass of material passing the 0.075mm sieve shall be determined in accordance with the requirements of AASHTO T-11

Table grading limits for graded clashed stone base course materials (GB1).

| Test sieve (mm) | Percentage by mass of total aggregate passing test sieve |
| --- | --- |
|  | Nominal maximum particle size |
|  | 37.5mm | 28mm | 20mm |
| 50 | 100 | - | - |
| 37.5 | 95-100 | 100 | - |
| 28 | - | - | 100 |
| 20 | 60-80 | 70-85 | 90-100 |
| 10 | 40-60 | 50-65 | 60-75 |
| 5 | 25-40 | 35-55 | 40-60 |
| 2.36 | 15-30 | 25-40 | 30-45 |
| 0.425 | 7-19 | 12-24 | 13-27 |
| 0.075 | 5-12 | 5-12 | 5-12 |

Note: - for pavers laid materials a lower fine content may be accepted.

B)Plasticity index

The fine fraction a GBI material shall be non plastic or shall have a maximum plasticity index of 6 when determined in accordance with AASHTO T-90

C)California Bearing ration (CBR)

The in-situ dry density of the placed material should be a minimum of 98% of the maximum dry density obtained in the ASTM test method D1557 (heavily compaction). The compacted thickness of each layer should not exceed 200mm.

Cursed stone base courses constructed with proper care with GB1 materials described above shoved have CBR values in excess if 100%

D)Aggregate Crushing Value (ACV)

Requirements expressed in terms of the values of the Aggregate crushing value (ACV) (British standard 812, part 110) may be used the ACV should preferably be less than 25% & in any case less than 29%.

Other simples tests the aggregate impact test (British standard 812, part 112 1990) may be used in quality control testing provided a relationship between the results of the choose test & the ten percent fines value (TFV) has been determined.

E)  Mechanical strength requirements (TFVT)

To ensure that the materials are sufficiently durable, they should satisfy the criteria given in table below these are a minimum ten percents fines value (TFV) (British standard 812, part III) and limits on the maximum loss in strength following a period of 24 hrs of soaking in water. The likely moisture conditions in the pavement are taken in to account in broad terms based on annual rainfall.

| Table:-mechanical strength requirement for the aggregate fraction of crushed stone based course materials (GB1) as defined by the ten percent fines test. Typical annual rain fall (mm) | Minimum 10% finesse values (KN) | Minimum ratio wet/Dry test (%) |
| --- | --- | --- |
| > 500 | 110 | 75 |
| < 500 | 110 | 60 |

# F) Flakiness index

The flakiness index shall not exceed 30% when determined in accordance with BS 812 part 105-1990.

6.11.2) Material requirements for naturally occurring granular materials                                       Boulders, weathered rock.

A)General

Graded natural gravel (GB2, GB3):

A wide range of materials including later tic, calcareous and quartzite gravels, river gravels, boulders and other transported gravels or granular material resulting from the weathering of rocks can be used successfully as base course materials the material shall be of such a natured that it can be readily transported, spread and compacted with out segregation.

B) Grading

The particle size distribution should be approximately parallel with the grading envelop, to ensure that the material has maximum mechanical stability, in the grading limits shown in table below when determined in accordance with the requirement of AASHTOT-27.

-	Recommended particle size distributions for mechanically stable natural gravels and weathered rocks for use as base course material (GB2, GB3)

|  | Nominal maximum particle size |
| --- | --- |
|  | 37.5mm | 20mm |
| 50 | 100 | - |
| 37.5 | 80-100 | 100 |
| 20 | 60-80 | 80-100 |
| 10 | 45-65 | 55-80 |
| 5 | 30-50 | 40-60 |
| 2.36 | 20-40 | 30-50 |
| 0.425 | 10-25 | 12-27 |
| 0.075 | 5-15 | 5-12 |

C)Plasticity index

A maximum index of 6 as for GB1if the PI approaches the upper limit of 6it is desirable that the fines content be restricted to the lower end of the range to ensure this, a maximum PP of 60 is recommended or alternatively a maximum plasticity modulus (pm) of go where .

Pm=PIX (percentage passing the 0.425mm sieve)

if difficulties are encountered in meeting  the plasticity criteria, consideration should be given to modifying the material by the addition of a low percentage of hydrated lime on cement.

D) Aggregate crushing value (ACV)

Minimum soaked 10% fines value (TFV) value. (B5 812, part 111) shall be

5O KN.

E) California bearing ratio (CBR)

When used as a base course, the material should be compacted to a density equal to or greater than 98% of the MDD achieved in the ASTM Test method D1557(heavy compaction)when compacted to this density in the laboratory, the material should have a minimum(CBR of 80%, after four days immersion in water (A55MD/1883).

### F) Abrasion

The loss Angeles abrasion value, determined by testing in accordance with AASHTO T96 shall not exceed 45 % at 500 revolutions unless otherwise specified in the prospect specifications.

G) Flakiness index.

The flakiness index shall not exceed 30%when determined in accordance with BS 812 part 105-1990

H)Crushed ratio

The crushed ratio shall be a minimum of 60%

I) Grading modulus

The minimum grading modulus for material once placed and compacted on the road shall be.

For natural material …2.0

For material to be chemically stabilized…..1.75

6.11.3) Material requirements for dense bitumen macadam

I) Coarse aggregate

The material shall consist of hard durable particles produced by crushing rock or boulders and shall be clean and free from organic mater, lumps of clay or other deleterious substances and complying with the requirements of AASHTO M-80.

Crushed rock or crushed boulders shall be produced from one or more of the following rock type.

Basalt Gabbros; Granite, Grit stone, Hornfels, Limestone, Porphyry or Quartzite,

A) Aggregate crushing value (ACV)

The aggregate crushing value of the coarse aggregate shall not exceed 25% when determined in accordance with BS812 part 3.

B)  Los Angeles abrasion

The Los Angeles abrasion value shall not exceed 35% when determined in accordance with the requirement of AASHTO T-96

C) Soundness

The loss of soundness of the coarse aggregate shall not be greater than 12% when tested in accordance with AASHTO T-104.

# D) Flakiness index

The flakiness index, shall not exceed 45% when determined in accordance with the requirements of BS 812 part 105-1990.

# E)Crushed ratio

The crushed ratio shall be a minimum of 100%

# F)Water absorption

The water absorption shall not exceed 2% when determined in accordance with requirements of AASHTO T-85.

# G)Coating of chippings

The coating of chippings with binder shall not be less than 60% when determined in accordance with the requirement of Pr EN 12 697-11:1998 E for compatibility between aggregate and bitumen.

II). Fine aggregate

Final aggregate shall comply with the requirements of AASHTO M-6 and shall consist of one of the following.

- Crushed rock of one of the following

- Natural sand

- A blend of i and ii above.

III). Filler

Where necessary to improve the combined or other properties of the mix, a filler of hydrated lime, cement or crushed rock or crushed boulder dust may be added. Filler shall be material passing the 0.07mm sieve. If used as an anti stripping agent, the quality of hydrated lime shall be at least 1.5% by weight of total aggregate and in no case shall the quantity exceed 3% by weight of total aggregate.

# IV). Binder

The binder shall be 60/70 penetration grade between complying with the requirements of AASHTO M-20.

# 6.12) Material requirements in mixed bitumen macadam

# A) Combined aggregate grading

The combined grading of the aggregates shall be a smooth continuous curve falling with in the grading limits shown in table 4 when determined in accordance with AASHTO T-27. The mass of material passing the 0.07mm sieve shall be determined in accordance with AASHTO T-11.

Table 4, combined aggregate grading limits for dense bitumen macadam

| Test sieve (mm) | %age by mass of total aggregate. Passing test sieve |
| --- | --- |
| 28 | 100 |
| 20 | 95-100 |
| 14 | 65-85 |
| 10 | 52-72 |
| 6.3 | 39-55 |
| 3.35 | 32-46 |
| 1.18 | - |
| 0.3 | 7-21 |
| 0.075 | 2-8 |

Notes:-

- When gavel other than limestone is used, the anti stripping properties shall be improved by including 2% Portland cement or hydrated lime in the material passing 0.075 mm sieve.

- Limestone and gravel shall not be used for wearing courses where high skidding resistance is required.

# B) Mix design parameters for dense between macadam

The parameters for dense between macadam, shall comply with the requirements as shown in table 5.

Table 5 mix design parameters for dense bitumen macadam

| Property | Unit | Value |
| --- | --- | --- |
| Bitumen content (percent by mass of total mix) | % | 5.0 ± 0.6 |
| Bitumen grade | Pen | 60/70 or 80/100 |
| Minimum Marshall stability (depending on design traffic) | KN | 3.5 - 9 |
| Flow | mm | 2 - 4 |
| Air voids | % | 4 - 8 |
| Voids in mineral aggregate | % | 16 - 22 |
| Voids filled with bitumen | % | 65 - 85 |
| Filler/bitumen ratio | % | 1 - 1.6 |
| Compaction level (depending on design traffic) | Number of blows | 2×50, 2×75 – to refusal |

Note:

- For aggregate with fine micro texture e.g. Limestone, the bitumen content should be reduced by 0.1 to 0.3%

- 60/70 grade bitumen is preferred.

6.13)  Materials for Embankment and Sub grades

AASHTO Designation M57-80(2000)

6.13.1Scope

This specification covers materials for use in the construction of embankments & sub grades.

6.13.2General Requirements

2.1. Materials shall be free from detrimental quantities of organic 	material, such as leaves, grass, roots, & sewage.

2.2. Material obtained from cuts or borrow areas shall conform to one of 	the following requirements.

Note.1 sees standard recommendation practice for the classification 	of soils & soil aggregate mixtures for Highway construction 	purpose (AASHTO M145)

2.2.1) In Embankments: Materials classified in the A-1, A-2-4, A-2-5-, or 	A-3 groups as in AASHTO shall be used when available & shall be compacted to the depth specified to not less than 95% of the maximum density per AASHTO T 99. If materials of this  character  is not  available & materials from the  A-2-6, A-2 -7, A-4, A-5, A-6, or A-7 groups must be used, special attention should be given to the design & construction of the embankment. Materials from these groups shall be compacted to  not less than 95% of the maximum density & within two percentage points of the optimum moisture 	content per AASHTO T 99.

2.2.2) In sub grads:- materials classified in the A-1, A-2-4, A-2-5, or A-3, groups as shown in AASHTO M-145  shall be used when a available & shall be compacted to not less than 95% of the maximum density  per AASHTO T 99. Materials in the A-2-6, A-2-7, A-4, A-5, A-6 or A-7 groups may be used if compacted to the depth specified not less than 95% of the maximum density & within two percentage points of the optimum moisture content per AASHTO T-99

2.3) Local shale may be used in embankment or sub grad construction if the condition of existing pavements & embankment indicate satisfactory results. Appropriate special specifications shall be prepared for such material.

6.13.3 Density Requirements

Density percentage requirements may be specified in terms of AASHTO T 180, provided the resultant density & optimum moisture content are comparable with AASHTO T-99 under the above conditions.

6.14 Fill materials /Soil or soil aggregate

- Sub grade: - it is the material below the pavement   & may include insitu material , fill or improved sub grade. These materials are used to support the pavement & shall have the following requirements:-

  - CBR value (100% MDD Standard compaction & four days soak) shall be more than 5%

  - Swell at 100% MDD Standard compaction & four days soak) less than 2%)

  - Organic matter (% by might ) <3%

2. Sub-base materials

These materials are naturally gravel soil mixtures, weathered rock etc. If transmits (distributes) the traffic load & shall fulfill the following requirements.

  - All materials shall have CBR at 95% MDD & four days soak, minimum 30%

  - Natural gravels

  - Max -size should be 2/3 layer thickness or 80mm which ever is the lesser.

  - Uniformity coefficient min = 5

  - Plasticity in index max = 15% in wet areas.

  - Gradation requirement shall be as follows under the title

"Materials for aggregate & soil   aggregate for sub base & surface course"

  - clayey & silty sands

  - Passing 2mm sieve, max 95%

  - Passing 0.075mm sieve 10% -30%.

  - uniformity coefficient > 5

  - Plasticity index in dry areas.5% - 20%

  - Plasticity index in net areas, 5 % - 12 %

3)Base materials

A base material is defined as any layer placed between the surface course & the sub grade. It may be an asphaltic concrete, black, base, crushed stone gravel, sand of low plasticity, fine grained material with a stabilizing additive etc. placement foundation layers are frequently separated in to two class, bases & sub bases. In general, the crushed stone & gravel bases,black bases & treated granular materials are considered as bases. Where as the less stable materials sands, fine gravels & treated sub grads are placed in the sub base category.

Materials for base shall have:-

  - CBR value> 80 % at  95 % AASHTO MDD (modified)

  - Los Angeles abrasion max 50%

  - Aggregate crushing val

  - Plasticity index max 6 %

  - liquid limit not more than 25 %

Grading requirement for base materials

Base course shall conform to ERA'S standard specification 200 below.

| Sieve size (mm) | Base | course |  |  | Surface | courses |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | C | D | E | F | G |
| 75 | 100 |  |  |  |  |  |  |
| 63 |  | 100 |  |  |  |  |  |
| 50 | 70-100 | 80-100 | 100 |  |  |  |  |
| 37.5 | 60-80 | 68-88 | 80-100 | 100 |  |  |  |
| 25 | 50-70 | 53-73 | 60-80 | 70-100 | 100 |  |  |
| 19 | 40-80 | 35-55 | 50-70 | 60-80 | 70-100 | 100 |  |
| 12.5 | - | - | - | 50-70 | 60-80 | 65-95 | 100 |
| 9.5 | 25-45 | 29-49 | 30-50 | 40-60 | 45-75 | 55-85 | 72-100 |
| 4.75 | 15-35 | 17-37 | 20-45 | 25-45 | 30-60 | 35-65 | 45-75 |
| 2.36 | - | - | - | - | - | - | - |
| 2.0 | 5-25 | 8-28 | 10-30 | 15-35 | 15-40 | 20-50 | 25-35 |
| 0.425 | 0-15 | 0-18 | 5-20 | 1-20 | 0-30 | 0-15 | 5-35 |
| 0.075 | 0-10 | 0-13 | 0-10 | 0-15 | 0-20 | 0-15 | 0-20 |

6.14) SURFACINGS

Prime coat & Tack coat

I- Prime Coat

A prime coat is an application of low viscosity bituminous binder to an absorbent surface. Its purposes are to waterproof the surface being sprayed & to help bind it to the overlying bituminous course.

- All non - bituminous road bases shall be primed.

- The most appropriate binders for priming are medium curing fluid cut-backs MC 30 & MC 70.

- MC 30 is suitable for practically all types of materials

- MC 70 is suitable only for open textured materials. Such as graded crushed stone.

- The rate of application will depend on the texture & density of the material to be primed. It is usually b/n 0.8 & 1.2 liters /m2

II- Tack Coat

A tack coat is a light application of bituminous binder to a bituminous on concrete surface. Its purpose is to provide a bond between the surface being sprayed & the overlying bituminous course.

The following types of bindery may be used

- Rapid curing cut-backs (RC 250,800 or 3000)

- Medium curing cut backs (MC 250,800 or 3000)

- Quick breaking emulations (Al or Kl ), or

- A3 Anomic emulation diluted with water 1:1

Note: MC 30 & MC 70 prime cut backs are not suitable for tack coats.

The rate of spray will depend on the surface texture. It is usually b/n 0.3 & 0.8 l/m2

6.14.1)Sizes of Aggregate for road & Bridge construction

AASHTO designation: M 43-88 (1999)

ASTM designation: D448-86(1993)

- Scope

1.1. This specification defines aggregate size designation & ranges in mechanical analyses for standard size of coarse aggregate & screenings for use in the construction & maintenance of various types of highways & bridges.

- Significance & Use

2.1 Contract documents may specify certain of these aggregate sizes for specific uses or may suggest one or more 0f these sizes as appropriate for the preparation of various end-product mixtures. In some cases, closer limits on variability of the aggregate grading may be required.

- Standard sizes

Standard sizes of coarse aggregate shall comply with the sizes given in table 1 sizes shall be determined by means of laboratory sieves having square openings & conforming to M 92.

6.14.2) Materials for Aggregate  & soil aggregate sub base   & surface course

AASHTO Designation: m 147-65 (2000)

1. Scope

This specification covers the quality & grading of sand-clay  mixtures: gravel, crushed stone of slag screenings: or sand  crushed run coarse aggregate consisting of gravel, crushed stone or slag with or without soil mortar or  any combination of these materials for use in the construction of sub base, base & surface courses. The requirements are intended to cover only materials having normal or average specific gravity, absorption & gradation characteristics. Where other materials are to be used appropriate limits suitable for there use must be specifies.

2.  General Requirements

2.1 Coarse Aggregate

2.1.1 Coarse aggregate retained on the 2.00 mm (No 10) sieve shall consist of hard, durable particles or  fragments of stone, gravel, or slag, materials that  break up when alternately frozen & thawed or wetted & dried shall not be used.

2.1.2 Coarse aggregate shall have a percentage of wear, by the loss Angels test, AASHTO T 96 of not more than 50

Note  1. A higher or lower percentage of wear may by specified by the engineer, dispending upon the materials available for the work.

2.2.1 Fine aggregate

2.2.1 Fine aggregate passing the 2.0mm (No.10) sieve shall consist of natural or crushed sand, & fine mineral particles passing the 75µm (No. 200 ) sieve

2.2.2 The fraction passing the75µm (No.200) sieve shall not be greater than two thirds of the fraction passing the 0.425mm (No.40) sieve. The fraction passing the 0.425mm sieve shall have a liquid limit not greater than 25 & a plastic index not less than 6.

2.3 All materials shall be free from vegetable matter & lumps or bonus of clay. The soil aggregate material shall conform to the grading requirements of Table 1.The grading requirements for composite aggregate material will be specified by the engineer.

Table 1 Grading Requirements for soil - aggregate materials

| sieve | Mass percent passing |
| --- | --- |
| Standard (mm) | Grading A | Grading B | Grading C | Grading D | Grading E | Grading F |
| 50 | 100 | 100 | - | - | - | - |
| 25 | - | 75-95 | 100 | 100 | 100 | 100 |
| 9.5 | 30-65 | 40-75 | 50-85 | 60-100 | - | - |
| 4.75 | 25-55 | 30-60 | 35-65 | 50-85 | 55-100 | 70-100 |
| 2.0 | 15-40 | 20-45 | 25-50 | 40-70 | 40-100 | 55-100 |
| 0.425 | 8-20 | 15-30 | 15-30 | 25-45 | 20-50 | 30-70 |
| 0.75 | 2-8 | 5-20 | 5-15 | 5-20 | 6-20 | 8-25 |

3)  Sub base Materials

3.1. Materials for sub base shall confirm to the requirement of sections 2 & 3 for Grading A, B, C, D, E, & F. The type & grading desired shall be specified.

4)   Base course Materials

4.1 Materials for base course shall conform to the requirements of section of for grading A, B, C, D, E or F. The grading desired Shall be specified.

5) Surface course materials

5.1 Materials of surface course shall conform to the requirements of section 2 & 3 for Grindings C, D, E, or F. The grading desired shall be specified.

Note: 1 Where it is planned that the soil aggregate surface course it to be maintained for several years without bituminous surface treatment or other superimposed imperious surfacing, the engineer of the minimum percentages shown in Table 1 for Grading C, D, or E. and should specify a maximum liquid limit of 35 & plasticity index range of 4 to 9 in lieu of the limits given in section 2.2.2

Note  2. For sub base & base coarse materials local experience has shown that lower percentages passing the 75NM (No 200 ) sieve than are required in table 1 are necessary for base course materials in order to prevent damage by frost action, the engineer should specify such lower percentages.

6. Moisture content

6.1 All materials shall contain moisture equal to or slightly below the optimum necessary to insure. That  the design density requirements are obtained when materials are compacted.

6.15) Viscosity - Grande Asphalt cement

AASHTO Designation: M 226-80 (2000)

1) Scope

This specification covers Asphalt comments graded by viscosity at 60 c (140F) for use in pavement constriction. Three sets of limits are offered in these specifications. The purchaser shall specify the applicable table of limits. In the events the purchaser does not specify limits, Table 1 shall apply. For asphalt cements graded by penetration at 25oc (77oF), See AASHTO M 20 for asphalt cement.

Table 1 Requirements for Asphalt cement Graded by viscosity at

60oc (140oF) Grading based on original Asphalt)

| Test | Viscosity Grade |
| --- | --- |
|  | Ac -2.5 Ac-5 Ac -10 Ac-20 Ac-40 |
| Viscosity, 60Oc, pa-s | 25±5 50±10 100±20 200±40 400±80 |
| Viscosity 135oc, mm2/s-min | 80 100 150 210 300 |
| Penetration, 25 oc | 200 120 70 40 20 |
| Flash point | 163 177 219 232 232 |
| Solubility in trichloroethylene | 99 99 99 99 99 |
| Test on residue from thin film oven test Viscosity, 60oc, pa.s | 100 200 400 800 1600 |
| Ductility, 25oc,5cm/min | 100 100 50 20 10 |
| Spot test (When & as specified ) with:- Standard naphtha solvent Naphtha xylene solvent, percent xylene Heptene - xylene solvent percent xylene-xylene –solevent % xylene | Negative for all grades Negative for all grades Negative for all grades |

1. If ductility is less than 100, material will be accepted if ductility at 15.6 oc) is 100 minimum.

2. The use of the spot test is optional (when it is specified)

2. Manufacture

The Asphalt cement shall be prepared for crude petroleum by suitable methods.

3. Requirements

3.1 The asphalt cement shall be homogeneous, free from water, & shall not form when heated to 175oC (3470F)

3.2 The asphalt cements shall conform to the requirements given in Table 1, 2,3 as specified by the purchaser.

Table 2 Requirements for Asphalt cement Graded by viscosity at 60 C (140) Grading based on original Asphalt)

| Test | Viscosity Grade |
| --- | --- |
|  | Ac -2.5 Ac-5 Ac -10 Ac-20 Ac-30 Ac-40 |
| Viscosity, 60oc, pa-s | 25±5 50±10 100±20 200±40 300±60 400±80 |
| Viscosity 135oc, mm | 125 175 250 300 350 400 |
| Penetration, 25 oc | 220 140 80 60 50 40 |
| Flash point oc | 163 177 219 232 232 232 |
| Solubility in trichloroethylene | 99 99 99 99 99 99 |
| Test on residue from thin film oven test Loss on heating % -max(optional ) | 1.0 0.5 0.5 0.5 0.5 |
| Viscosity, 60oc, pa.s | 100 200 400 800 1200 1600 |
| Ductility, 25 oc | 100 100 75 50 40 25 |

Table 3 Requirements for Asphalt cement Graded by viscosity at 60 C (Grading based on Rolling thin film oven Test)

| Test on residue from AASHTO Test method T-240 | Viscosity Grade |
| --- | --- |
|  | AR-10 AR-20 AR-40 AR-80 AR-160 |
| Viscosity, 60oc, pa-s | 100±25 200±50 400±100 800±200 1600±400 |
| Viscosity, 135oc, mm2/s-min | 140 200 275 400 550 |
| Penetration, 25 oc,100g ,5sec | 65 40 25 20 20 |
| Percent of original pen.25 oc-min | - 40 45 50 52 |
| Ductility ,25 oc 5cm/min | 100 100 75 75 75 |
| Test on organic asphalt Flash point oc | 205 219 227 232 238 |
| Solubility in trichloroethylene % | 99 99 99 99 99 |

1. AASHTO T 179 (Thin - film oven test) may be used, but AASHTOT 240 shall be the referee method.

2. If ductility is less than, material will be accepted if ductility at 15.6 oc is 100 minimum.

6.16) Standard specification for cut-Back Asphalt (medium-curing type)

AASHTO Designation m -82 - 75 (2000)

1) Scope

This specification covers liquid petroleum products, produced by fluxing an asphaltic base with suitable petroleum distillates, to be used  in the treatment of road surfaces.

2. General Requirements

The cut back Asphalt shall show no separation 02 curdling prior to use & shall not foam when heated to the application temperature.

3) Properties

Cut-back asphalt of the grade designated shall confirm to the requirements shown in Table1

|  | Mc-30 | Mc-70 | Mc-250 | Mc-800 | Mc-3000 |
| --- | --- | --- | --- | --- | --- |
|  | Min max | Min max | Min max | Min max | Min max |
| Kinematics viscosity at 60oc, mm 2/s | 30 60 | 70 140 | 250 500 | 800 1600 | 3000 6000 |
| Flash point (Tag, open cup) | 38 - | 38 - | 66 - | 66 - | 66 - |
| Water, % | - 0.2 | - 0.2 | - 0.2 | - 0.2 | - 0.2 |
| distillation test |  |  |  |  |  |
| distillate to 360 oc |  |  |  |  |  |
| to 225 oc | - 25 | 0 20 | 0 10 | - | - |
| to260 oc | 40 70 | 20 60 | 15 55 | 0 35 | 0 15 |
| to 315 oc | 75 93 | 65 90 | 60 87 | 45 80 | 15 75 |
| Residue from distillation of 360 |  |  |  |  |  |
| volume % of sample by difference | 50 - | 55 - | 67 - | 75 - | 80 - |
| Tests on residue from distillation |  |  |  |  |  |
| Absolute viscosity at 60 oc Pa.s | 30 120 | 30 120 | 30 120 | 30 120 | 30 120 |
| Ductility, 5cm(min, | 100 - | 100 - | 100 - | 100 - | 100 - |
| Solubility in trichloroethylene. | 99 - | 99 - | 99 - | 99 - | 99 - |
| spot test (see note 3) with |  |  |  |  |  |
| Standard naphtha | Negative for all value » » |
| Naphtha -xyene solvent % xylene |  |
| Heptanes -xylene solventa % xytene |  |

Note 1  As an alternate, say bolt -Furol Viscosities may be specified as fallows

Grade MC- 70 Fural Viscosity at 50 co 60 co to 120se

Grade MC -30 Fural Viscosity at 25 co -75 co to 150se

Grade MC -250 Fural Viscosity at 60 co -125 co to 250se

Grade MC -800- Furol Viscosity at 82.2 co -100 co to 200se

Grade MC -3000 - Furol viscosity at 82.2 co c -300 co to 600se

Note 2 :- If the ductility at 25oc is less than100, the material will be acceptable if its ductility at 15.5oc  is more than 100.

Note 3: The use of the spot test is optional, when specified, the engineer shall indicate whether the standard naphtha  solvent, the naphtha - xylene solvent or the heptane -xylene solvent will be used in determining compliance wish the requirement, & also, in the case of the xylene solvents, the percentage of xylene to be used.

Note 4: in view of Viscosity of the residue, the specifying agency, at its option, can specify penetration at 100, see at for Grades MC-70,MC-250,Mc-800,& Mc -3000.  However, in no case will both be required.

6.17) Standard specification for Emulsified Asphalt

ASTM D977-97

1) Scope

This   specification covers twelve grades of emulsified Asphalt for use in pavement construction in the manner designated.

2. Requirements.

2.1 The emulsified asphalt shall be tested within 14 days of delivery. The emulsified asphalt shall be homogeneous after through mixing provided separation has not been caused by freezing. Emulsified asphalts separated by freezing shall not be tested.

2.2 Emulsified Asphalt shall conform to the requirements prescribed inTable 1

Table 1 requirement for Emulsified Asphalt

| Type | Rapid setting | Medium - setting |
| --- | --- | --- |
| Grade | RS-1 | RS-1 | R/F RS-2 | Ms-1 | Ms-2 | Ms-3 |
|  | Min. max | Min max | Max Min | Max Min | Max min | Max Min |
| Tests on emulsions: Velocity , say bolt furol at 50 | - - | 75 400 | 75 400 |  |  |  |
| Storage stability test 24-h | - 1 | - 1 | - 1 | - 1 | - 1 | - 1 |
| Demulsibility,35ml, 0.02N cacl2% | 60 - | 60 - | 60 - | 60 - | 60 - | 60 - |
| Coating ability & water resistance: |
| Coating dry aggregate | - | - | - | good | good | good |
| Coating after spraying |  |  |  | Fair | Fair | Fair |
| Coating wet aggregate |  |  |  | Fair | Fair | Fair |
| cement mixing testing % | - | - | - | - | - | - |
| sieve test, % | - 0.1 | - 0.1 | - 0.1 | - 0.1 | - 0.1 | - 0.1 |
| Residue by destination % | 55 - | 63 - | 63 - | 55 - | 65 - | 65 - |
| oil distillate by volume of emulsion % Tests on residue from distillation test |
| Penetration, 25oc, 100g 5 second | 100 200 | 100 200 | 400 900 | 100 200 | 100 200 | 40 90 |
| Ductility,25 oc | 40 - | 40 - | 40 - | 40 - | 40 - | 40 - |
| Solubility ininichloro ethylene,% | 97.5 - | 97.5 - | 97.5 - | 97.5 - | 97.5 - | 97.5 - |
| Tests on emersions |
| Viscosity, say bolt furol at 25 oc | 20 100 | - - | - - | 20 100 | 100 - | 100 - |

| Type | Rapid setting | Medium - setting |
| --- | --- | --- |
|  | HFAASI-1 | HFMS-2 | HFMS-2h | HFMS-25 | SS-1 | SS-1h |
| Grade | Min max | min max | Min max | Min max | Min max | min max |
| Tests on emulsions: |
| Velocity , say bolt furol at 50 | 20 200 | 100 - | 100 | 50 | 20 100 | 20 100 |
| Storage stability test 24-h | - 1 | - 1 | - 1 | - 1 | - 1 | - 1 |
| Demulsibility, 35ml, 0.02N cau% |  |  |  |  |  |  |
| Coating ability & water resistance: |  |
| Coating dry aggregate | good | good | good | good | - | - |
| Coating after spraying | Fair | Fair | Fair | Fair | - | - |
| Coating wet aggregate | Fair | Fair | Fair | Fair | - | - |
| Coating after spraying | Fair | Fair | Fair | Fair | - | - |
| coment mixing test, % | - - | - - | - - | - - | - 2.0 | - 2.0 |
| sieve test, % | 0.1 - | 0.1 - | 0.1 - | 0.1 - | 0.1 - | 0.1 - |
| Residue by destination % | 55 - | 65 - | 65 - | 65 - | 57 - | 57 - |
| oil distillate by volume of emulsion % | - - | - - | - - | 1 7 | - - | - - |
| Tests on residue from distillation test |
| Penetration, 25c, 100g | 100 200 | 100 200 | 40 90 | 200 | 100 200 | 40 90 |
| Ductility,25 | 40 - | 40 - | 40 - | 40 - | 40 - | 40 - |
| solubility in inichloro ethylene,% | 97.5 | 97.5 | 97.5 | 97.5 | 97.5 | 97.5 - |
| Float test, 60oc, s | 1200 - | 1200 - | 1200 - | 1200 - | -- - | - - |

6.18) Standard specification for Emulsified Asphalt

AASHTO Designation M 140 -88 (1998)

AASHTO M 140-88 (1998) is identical to ASTM D977 -97 except for the following provisions

1) Replace section 2.1 of ASTM D977 with the following:

2.1) The emulsified Asphalt shall be homogeneous. Within 30days after delivery & provided separation has not been caused by greezing, the emusifed asphalt shall be homogeneous after through mixing.

2. Add the following footnotes to the end of table 1 of ASTM D977 -97 as follows:

b) Remissibility - The deducibility test shall be made within 30 days from date of shipments.

C. Sieve Test - A percentage of 0.3 is acceptable for samples taken at print of use

d) Refer to AASHT  RS for typical applications.

6.18.1) Penetration Graded Asphalt Cement

AASHTD designation: m20 - 70 (2000)

1)Scope

This specification covers the following five penetration grades of Asphalt coment for use in highway construction : 40 to 50, 60 to 70, 85 to 100, 120 to 150, & 200 to 300 . For Asphalt cement graded by viscosity, see AASH to m 226

2. Manufacture

Asphalt cement shall be prepared by the refining of crude petrolium by suitable methods.

3) Properties

3.1 The Asphalt cement shall be homogeneous, free from water, & shall not foam when heated to 175c (374 F)

3.2 The various grades of asphalt shall conform to the requirements given in Table 1

Table 1 Requirements for a specification for asphalt cement.

| Penetration grade |
| --- |
|  | 40 -50 | 60-70 | 85-100 | 120-150 | 200-300 |
|  | Min max | Min max | Min max | Min max | Min max |
| Penetration at 250c (77oc) 100g, 5sec | 40 50 | 60 70 | 80 100 | 120 150 | 200 300 |
| Flash point, cleveland open cup,oc | 232 - | 232 - | 232 - | 218 - | 177 - |
| Ductility at 25c(77) 5cm per min, cm | 100 - | 100 - | 100 - | 100 - | 100 - |
| Solubility in trichloro ethylene percent | 99 - | 99 - | 99 - | 99 - | 99 - |
| Thin - film over test, 3.2mm,163c,5hr |  |  |  |  |  |
| Loss on heating, percent | - 0.8 | - 0.8 | - 0.8 | - 0.8 | - 0.8 |
| Ductility of residue at 25c, 5cm /min, cm | - - | 50 - | 75 - | 100 - | 100 - |
| Penetration, of residue, percent of original | 58 - | 54 - | 50 - | 46 - | 40 - |
| Spot test (when & as specified (see note ) with): |
| Standard Naphthe solvent | Negative for all grades |
| Naphtha xylene solvent, percent xylent | Negative for all grades |
| Heptane - xylene solvent, percent xylene | Negative for all grades |

6.19   BITUMINOUS PRIME COAT

(ERA 2000)

1. SCOPE

This Division covers the application of a bituminous prime coat to a prepared pavement

layer.

2 MATERIALS

(a) Priming material

The priming material shall be one of the following as specified or as directed by the

Engineer:

MC-30, MC-70, or MC-250 cutback bitumen complying with AASHTO M 81 or M 82, as applicable;

Invert bitumen emulsion complying with SABS 1260

(b) Mineral Aggregate for Blinding

The aggregate used for blinding the primed surface shall consist of crushed rock or river

Sand, with 100% passing the 6.7 mm sieve and not more than 10% passing the 2.36 mm

Sieve. The aggregate shall be clean, hard and free from excessive dust. It shall contain no

clay, loam, or other deleterious matter.

(c) Air blowers

Air blowers or compressors shall be designed and operated to assist in the removal of loose or deleterious material from the surface of pavement layers.

3 WEATHER AND OTHER LIMITATIONS

No prime shall be applied under the following adverse conditions:

(a) During foggy or wet conditions;

(b) When rain is imminent;

(c) When wind is sufficiently strong to cause uneven spraying;

(d) When the surface of the layer is wet, i.e. more than damp;

(e) When at any position the moisture content of the top 25 mm of the layer to be

Primed is greater than 50% of the optimum moisture content of the material in the layer;

(f) When the temperature of the surface immediately prior to commencing the application of the prime is below or, in the opinion of the Engineer, likely to fall below 100 C;

(g) After sunset.

The Engineer's decision on whether or not to apply the prime coat under specific weather

Conditions shall be final.

6.20)  TACK COAT

SCOPE

This Division covers the specification of materials for, and the application of bituminous

tack coats to prepared pavement layers or surfacing.

MATERIALS

(a) Tack coat material

The material used for tack coats shall be one of the following as specified or as directed by the Engineer:

(i) RC-70 cutback bitumen complying with AASHTO M 81 or M 82, as applicable;

(ii) Bitumen emulsion complying with AASHTO M-140 or M-208.

(b) Water for the Production of Bitumen Emulsion (emulsified asphalt)

Water used for the production of bitumen emulsion (emulsified asphalt) shall comply with the requirements of water quality type A.

c) WEATHERANDOTHER LIMITATIONS

No tack coat shall be applied under the following adverse conditions:

(a) During foggy or wet conditions;

(b) When rain is imminent;

(c) When wind is sufficiently strong to cause uneven spraying;

(d) When the surface of the layer is wet or damp;

(e) When the temperature of the surface of the layer immediately prior to commencing

the application of the tack coat is below 200 C;

(f) When the air temperature immediately prior to commencing the application of the

tack coat is below or, in the opinion of the Engineer, likely to fall below 100 C;

(g) after sunset.

The Engineer's decision on whether or not to apply the tack coat under specific weather

conditions shall be final.

6.21) SURFACE TREATMENTS: MATERIALS

AND GENERAL REQUIREMENTS

01 SCOPE

This Division covers the materials, constructional equipment, and construction methods and requirements common to the construction of all surface treatments specified in these

Specifications.

02 MATERIALS

(a) Bituminous Binders

The type and grade of bituminous binder to be used shall be that specified under the

appropriate Division of these Specifications for each type of bituminous surface treatment, or in the Project Specifications, or as ordered by the Engineer.

Duplicate delivery slips shall accompany each load of bituminous material and shall contain the name of the producer and the supplier, the type and grade of material, the loading temperature of the material, and the lot number and date of approval of the material from which delivery is made. When considered necessary by the Engineer and at his sole discretion, a time limit may be imposed between the date of approval and the date of delivery, or between the date of approval and the date of use in the Works..

The Contractor shall provide to the Engineer certificates issued by all suppliers of

bituminous binders to the effect that the binders delivered to the Site comply with the test

Requirements specified in the relevant specifications. The cost such tests shall be borne as specified The Engineer shall have the authority to order the Contractor to have the bituminous binders tested by an approved laboratory for compliance with all or any of the requirements specified and the results of such tests shall be submitted directly by the testing laboratory to the Engineer with copies if requested to the Contractor.

(i) Conventional Bituminous Binders

Bituminous binders shall comply with the following specifications:

(i) Penetration-grade bitumen AASHTO M 20

(ii) Cutback bitumen AASHTO M 82

(iii) Anionic bitumen emulsions (emulsified asphalts) AASHTO M 140

(iv) Cationic bitumen emulsions (emulsified asphalts) AASHTO M 208

Spray-grade bitumen emulsions shall be subject to the following viscosity requirements:

(1) Anionic spray-grade emulsion (60 %): minimum 12 degrees Engler at 20OC

(2)) Cationic spray-grade emulsion (60, 65, 70 %): minimum 80 seconds Saybolt Furol at 50O C

(ii) Non-homogeneous (heterogeneous) Modified Bituminous Binders (summer grade)

Bitumen-rubber binders shall comply with the following requirements:

(1) Base bitumen

The bituminous binder used in the production of the bitumen-rubber shall be a

60/70, 80/100 or 150/200 penetration-grade bitumen or a blend of approved grades

to provide a product with the required viscosity properties.

(2) Rubber

Rubber shall be obtained by processing and recycling pneumatic tyres.

The rubber crumbs shall be produced by a mechanical comminuting process. Crumbs produced by cryogenic-mechanical techniques shall not be used. It shall be pulverized, free from fabric, steel cord and other contaminants. A maximum of 4% by mass of fine

particle size calcium carbonate, or talc, may be added to the rubber crumbs to prevent the rubber particles coalescing. At the time of use the crumbs shall be free flowing and dry and comply with the requirements of table /1.

Table 1 Rubber Crumbs

| Sieve Analysis |
| --- |
| Sieve size(mm) | % passing by mass | Test method |
| 1.18 | 100 | sabita,BR6T |
| 0.60 | 40-70 |  |
| 0.075 | 0-5 |  |
| Other Requirements |  |
| Natural rubber hydrocarbon content | 30% (minimum) | BS 903,parts B 11 & B 12 |
| Fbre length (mm) | 6mm(maximum) |  |
| Relative density(g/cm2) | 1.10-1.25 | Sabita, BR9T |

(3) Extender oils

Extender oil shall be petroleum-derived material of high aromatic and shall

Comply with the requirements of table 6300A/2.

Table /2 Extender Oils

| Property | Requirements |
| --- | --- |
| Flash Point | 180O C (minimum |
| Saturated Hydrocarbons by mass | 25% (maximum) |
| Un-saturated Hydrocarbons by mass | 55% (minimum) |

(4) Diluents

Diluents shall be a hydrocarbon distillate.

(5) Bitumen-rubber blend

The bitumen-rubber blend, including extender oil and/or diluents (if necessary),

shall comply with the requirements of table /3.Prior to commencement of the work, the supplier shall state in writing the percentage of rubber and the blending/reaction temperature he intends to use for his specific product. The actual percentage of rubber shall not deviate by more than 1% from the stated value and the actual reaction temperature shall not deviate by more than 10% from the stated value.

A continuous record of both percentage of rubber added and reaction temperatures

shall be kept on site by the Contractor.

The bitumen-rubber binder shall comply with the requirements of table /4.In order to determine the final process and the acceptance limits, the contractor shall provide the engineer with time-temperature ratios in regard to the above properties of the specific product before work may start.

The methods of testing bitumen-rubber material have been published in Manual 3

of the Southern African Bitumen and Tar Association.

If a diluents is used, an ageing test may be required in which the binder is placed in

an oven for 5 hours at 150o C, after which time it shall comply with the above

specifications.

The contractor shall provide the performance record of the materials he intends to

use for three recent projects in order to assess the successful use of the materials.

The information shall include mean values obtained for the prescribed tests as well

as any relevant comments. This information shall be submitted at tender stage.

Table /3 Bitumen- Rubber Blend

| Property | Requirements |
| --- | --- |
| Rubber content of the total blend by mass | 20% - 40% |
| Extender oil content of the total blend by mass | 6% (maximum |
| Diluents content of the total blend by mass | 7% (maximum) |
| Blending/reaction temperature | 170O - 210O C |
| Reaction time | 0.5 – 4.0 hours |

Table/4 Bitumen- Rubber Binder

| Property | Requirements | Test Method |
| --- | --- | --- |
| Compression recovery: after 5 minutes after 1 hour after 4 hours | 70% (minimum) 70% (minimum) 48% - 55% (minimum | BR6T (Sabita) |
| Ring-and-ball softening point | 55O C (minimum) | ASTM D 36 |
| Resilience (%) | 13% - 35% (minimum | Sabita, BR2T |
| Dynamic viscosity (Haake at 190O C) | 20 – 35 dPa.s | Sabita, BR5T |
| Flow | 20mm– 75 mm | Sabita, BR4T |

(iii) Non-homogeneous modified binders (winter grade)

If non-homogeneous modified binders (winter grade) are required, they shall comply with

the requirements in the project specifications.

(iv) Homogeneous cold applied modified binders

If any polymer other than the elastomer polymers styrene-butadiene rubber (SBR) or

styrene-butadiene (SBS) is required for the manufacture of cationic modified bitumen

emulsions it shall comply with the requirements in the project specifications.

Where applicable the following details will be indicated in the project specifications:

(1) Elastomer polymer type: SBR or SBS. Unless otherwise specified SBR shall

be used for tender purposes.

(2) base bitumen grade: 80/100 or 150/200 penetration-grade bitumen.

Unless otherwise specified 80/100 penetration-grade bitumen shall be used for tender

purposes.

(3) modified binder content: 65% or 70%. Unless otherwise specified 65% shall

be used for tender purposes.

Unless otherwise specified, the properties of cationic modified bitumen emulsion containing

SBR or SBS solids shall comply with the requirements in table /5

.

Table /5 Cationic Modified Bitumen Emulsion

| Property | Requirements | Test Method |
| --- | --- | --- |
|  | Polymer Modifier |  |
|  | SBR | SBS |  |
| Base bitumen (penetration-grade | 80/100 | 150/200 | 80/100 | 150/200 |  |
| Minimum modified binder content(%) | 70 | 65 | 70 | 65 | ASTM D 244 |
| Minimum viscosity at 50O C Saybolt Furol (seconds) | 80 | 70 | 80 | 50 | ASTM D 244 |
| Maximum residue on sieving (g/100 ml) | 0.25 | 0.25 | 0.25 | 0.25 | SABS 548 |
| Particle charge | Positive | Positive | Positive | Positive | SABS 548 |
| Sedimentation after 60 rotations | Nil | Nil | Nil | Nil | SABS 548 |

The properties of the modified bitumen recovered by using a rotary vacuum evaporation

Method or simple evaporation method as described in Technical Guidelines for Seals using homogeneous modified Binders, Sabita Manual 15, May 1994, shall comply with the requirements of table /6.

Table /6 Recovered Modified Bitumen

| Property | Requirements | Test Method |
| --- | --- | --- |
|  | Polymer Modifier |  |
|  | SBR | SBS |  |
| Grade of base bitumen (penetration-grade) | 80/100 | 150/200 | 80/100 | 150/200 |  |
| Minimum softening point (O C) | 55 | 45 | 60 | 47 | ASTM D 36 |
| Minimum dynamic viscosity at 135O C (Pa.s) | 1.3 | 1.0 | 1.3 | 1.0 | ASTM D 4402 |
| Maximum residue on sieving (g/100 ml) | 0.25 | 0.25 | 0.25 | 0.25 | SABS 548 |
| Minimum ductility at 10O C (mm) | 1000 | 1000 | 500 | 500 | DIN 52013 |
| Minimum elastic recovery (ductilometer) at 10O C (%) | 52 | 55 | 55 | 60 | DIN 52013 |
| Minimum adhesion at 5O C (%) Minimum adhesion at 50O C (%) | 90 100 | 90 100 | 90 100 | 90 100 | Modified Vialit |

(v) Homogeneous hot-applied modified binders (summer grades)

The requirements for any polymer other than the generic types listed in table 6300A/7 used for the manufacture of homogeneous hot-applied modified binders will be indicated in the project specifications.

Where applicable the following details will be indicated in the project specifications:

(1) Generic polymer type: (plastomer or elastomer). Unless otherwise specified

elastomer type shall be used for tender purposes.

(2) Base bitumen grade: (80/100 or 150/200 penetration-grade bitumen). Unless

otherwise specified 80/100 penetration-grade bitumen shall be used for tender

purposes.

Table /7 Hot-applied Modified Binders

| Property | Requirements | Test Method |
| --- | --- | --- |
|  | Plastomer Polymer (EVA) | Elastomer Polymer |  |
|  |  | SBR | SBS | SBR | SBS |  |
| Grade of base bitumen (penetration-grade) | 150/200 | 80/100 | 150/200 |  |
| Minimum softening point (Ring & Ball) (O C) | 48 | 47 | 49 | 45 | 47 | ASTM D 36 |
| Minimum dynamic viscosity at 135O C (Pa.s) | 0.5 | 1.0 | 0.5 | ASTM D 4402 |
| Minimum ductility at 10O C (mm) | 300 | 1000 | 500 | 1000 | 500 | DIN 52013 |
| Minimum elastic recovery (ductilometer) at 10O C (%) | 45 | 55 | 60 | 55 | 60 | DIN 52013 |
| Maximum stability difference (Ring & Ball) (O C) | 2 | 2 | 2 | DIN 52013 |
| Minimum adhesion at 5OC (%) Minimum adhesion at 50OC (%) | 90 | 90 100 | 90 | 90 | 90 100 | Modified Vialit |

(vi) Homogeneous hot-applied modified binders (winter grade)

Where applicable the requirements for homogeneous modified binders (winter grade) will

be specified in the project specifications.

(b) Water for the production of bitumen emulsion

Water used for the production of bitumen emulsion shall comply with the requirements of

water quality type A.

(c) Chippings for Surface Treatments

The material for chippings shall consist of approved crushed stone, crushed boulders or

crushed gravels. The crushing ratio shall be 100 %. The material shall be free from clay

balls and adherent films of clay or other matter that would prevent thorough coating with

bituminous material. It shall be of such nature that after being coated thoroughly with

bituminous material of the type to be used in the work, over 95 percent of the bituminous

material will be retained after being subjected to a stripping test in accordance with

AASHTO T 182. The grading, hardness and shape shall be as follows for each nominal size of stone:

(i) Grading

The grading shall comply with the requirements set out in Table/8. The nominal size or sizes shall be as specified in these Specifications and the Project Specifications.

Table /8 Single Sized Crushed Aggregate Grades 1, 2 and 3

| Sieve size (mm) | Grade | Percentage passing by mass |
| --- | --- | --- |
| 37.5 |  | Nominal maximum size (mm) |
| 26.5 |  | 26.5 | 19.0 | 13.2 | 9.5 | 6.7 | 4.75 | 2.36 |
| 19.0 | Grades 1 &2 | 100 |  |  |  |  |  |  |
| 13.2 |  | 85-100 | 100 |  |  |  |  |  |
| 9.5 |  | 0-30 | 85-100 | 100 |  |  |  |  |
| 13.2 |  | 0-5 | 0-30 | 85-100 | 100 |  |  |  |
| 9.5 |  |  | 0-5 | 0-30 | 85-100 | 100 |  |  |
| 6.7 |  |  |  | 0-5 | 0-30 | 85-100 | 100 |  |
| 4.75 |  |  |  |  | 0-5 | 0-30 | 85-100 | 100 |
| 3.35 |  |  |  |  |  |  | 0-30 |  |
| 2.36 |  |  |  |  |  | 0-5 | 0-5 | 0-100 |
|  | Grade 3 | As grades 1 & 2 except: * 0 – 50; ** 0 - 10 |
| 0.425 | Grade 1 | < = 0.5 | < = 0.5 | < = 0.5 | < = 0.5 | < = 0.5 | <= 1.0 | <= 15.0 |
|  | Grade 2 | <= 1.5 | <= 1.5 | <= 1.5 | <= 1.5 | <= 2.0 | <= 2.5 | <= 15.0 |
|  | Grade 3 | N/A | N/A | <= 2.0 | <= 2.0 | <= 3.0 | <= 3.5 | <= 15.0 |
| 0.075 | Grade 1 | N/A | N/A | N/A | N/A | N/A | N/A | <= 2.0 |
|  | Grade 2 | < = 0.5 | < = 0.5 | < = 0.5 | < = 0.5 | <= 1.0 | <= 1.0 | <= 2.0 |
|  | Grade 3 | N/A | N/A | <= 1.5 | <= 1.5 | <= 1.5 | <= 1.5 | <= 2.0 |

Table /9 Sands for Surface Treatments

| Sieve Size (mm) | Percentage passing by mass |
| --- | --- |
|  | Texture Improvement | Sand seal | Grit Seal |
| 6.7 | - | - | - |
| 4.75 | - | - | 100 |
| 2.36 | - | 100 | 0-100 |
| 1.18 | 100 | 0-80 | 0-50 |
| 0.60 | 82-100 | 0-40 | 0-20 |
| 0.30 | 50-70 | 0-15 | 0-10 |
| 0.15 | 20-35 | 0-2 | 0-5 |
| 0.075 | 7-15 | - | 0-2 |
| Sand Equivalent (%) | >= 35 |

(ii) Hardness

The Los Angeles Abrasion value, determined by testing in accordance with AASHTO T96shall not exceed 30 at 500 revolutions unless otherwise indicated in the project

specifications.

The 10% FACT value (dry) shall be at least 210 kN and the wet to dry ratio shall be at least 75%.

The polished stone value (PSV) shall be at least 50 unless otherwise indicated in the project specifications.

(iii) Shape

The flakiness index, determined by testing in accordance with BS812, Part 105 or ASTM D3398, shall not exceed the values in Table /10.

Table /10 Flakiness Index

| Nominal Size (mm) | Maximum Flakiness Index% |
| --- | --- |
|  | Grade 1 | Grades 2 & 3 |
| 19.0 | 25 | 30 |
| 13.2 | 25 | 30 |
| 9.5 | 30 | 35 |
| 6.7 | 30 | 35 |

If so required for special purposes the average least dimension (ALD) shall be as indicated in the project specifications.

(iv) Soundness

The sodium sulfate soundness value, determined by testing in accordance with AASHTOT 104, shall not exceed 12.

(d) Aggregates for Slurry Seal

The aggregate for slurry seal shall be approved crusher sand obtained from a parent rock

having a Los Angeles Abrasion value not exceeding 40 or a mixture of crusher sand and

approved clean natural sand where the mixture contains not more than 25% of natural sand.

The aggregate shall be clean, tough, durable, angular in shape, and shall conform to the

following grading requirements:

Table /11 Aggregates for Slurry Seals

| Sieve size (mm) | Percentage passing by mass |
| --- | --- |
|  | Fine Slurry | Coarse Slurry |
|  | Fine | Medium | Coarse | Type1 | Type 2 |
| 13.2 |  |  |  |  | 100 |
| 9.5 |  |  |  | 100 | 85-100 |
| 6.7 |  | 100 | 100 | 85-100 | 70-90 |
| 4.75 | 100 | 90-100 | 70-90 | 70-90 | 60-80 |
| 2.36 | 90-100 | 65-90 | 45-70 | 45-70 | 40-60 |
| 1.18 | 65-90 | 45-70 | 28-50 | 25-45 | 25-45 |
| 0.6 | 40-60 | 30-50 | 19-34 | 15-30 | 15-30 |
| 0.30 | 25-42 | 18-30 | 12-25 | 10-20 | 10-20 |
| 0.15 | 15-30 | 10-21 | 7-18 | 6-15 | 6-15 |
| 0.075 | 10-20 | 5-15 | 1-5-15 | 4-10 | 4-10 |  |
| Sand equivalent | >= 35 |
| ACV | <=30 |
| Bitumen content (% by mass of dry aggregate | 10.0 – 16.0 | 7.5 – 13.5 | 6.5 – 12.0 |  |  |

.

Table /12 Aggregates for Rapid Setting Slurry Seals

| Sieve size (mm) | Nominal maximum size (mm) |
| --- | --- |
|  | 4.75 | 6.7 | 9.5 | 13.2 |
|  | Overlays | Rut Filling |
|  | Percentage passing by mass |
| 13.2 |  |  |  | 100 |
| 9.5 |  |  | 100 | 80-100 |
| 6.7 |  | 100 | 66-100 | 60-84 |
| 4.75 | 100 | 70-100 | 57-75 | 50-70 |
| 3.35 | 80-100 | 50-75 | 48-85 | 44-62 |
| 2.36 | 64-80 | 46-60 | 42-56 | 38-57 |
| 1.18 | 40-55 | 32-47 | 28-43 | 28-43 |
| 0.60 | 27-38 | 20-34 | 18-33 | 18-33 |
| 0.30 | 14-24 | 10-22 | 10-20 | 10-20 |
| 0.15 | 9-18 | 7-14 | 7-14 | 7-14 |
| 0.075 | 5-15 | 5-10 | 5-10 | 5-10 |
| Sand Equivalent (%) | >= 35 |
| Modified Emulsion (litres/m3) | 200 | 190 | 160 | 150 |

(e) Cement Filler for Slurry Seal

Portland cement shall comply with the requirements of AASHTO M 85 or equivalent grade in accordance with ISO or Ethiopian Standards.

Road lime shall comply with the requirements of AASHTO M 216 (lime for stabilization).

One filler shall be used throughout in order to minimize co lour differences in the surface.

(f) Hydrophillic aggregates

Where hydrophilic or other problematic aggregates are encountered, the Engineer may

order that the chippings be pre-coated as described below,

(i) Pre-coating of aggregate for stockpiling or immediate use

The untreated aggregate shall be thoroughly wetted and allowed to drain off to a damp

condition. An approved pre-coating fluid (containing an approved wetting agent (eg

Duomene T or similar at a rate of 0.5 % by volume of the pre-coating fluid) shall be applied at the rate of 12 liters per cubic meter of aggregate. The mixture of pre-coating fluid and aggregate shall be suitably agitated, turned and mixed until the aggregate is uniformly coated with the pre-coating fluid.

(ii) Stockpiling

Areas used for stockpiling pre-coated aggregates shall be so sited to minimize the deposition of dust on the aggregates. Where necessary adjacent roads or diversions shall be watered or sealed. When there is a danger that the pre-coating fluid will be washed off by rain the stockpiles shall be covered with tarpaulins or similar protective coverings.

(iii) Binders

No pre-coating shall be applied where conventional and modified emulsion binders are to be used unless specified or ordered by the Engineer.

(iv) Time limit

The time between the pre-coating and the placing of the aggregate shall not exceed the time specified in the project specification or as agreed by the Engineer.

MC-800 10

MC-3000 10

Bitumen emulsions 10

(ii) Non-homogeneous modified binders (summer grade)

Bitumen-rubber (spray application) 25

(iii) Non-homogeneous modified binders (winter grade)

As specified in the project specification

(iv) Homogeneous cold-applied modified binders

SBR modified cationic emulsion 10

SBS modified cationic emulsion 10

(v) Homogeneous hot-applied modified binders (summer grade)

Modified 150/200 penetration grade 21

Modified 80/100 penetration grade 25

(vi) Homogeneous hot-applied modified binders (winter grade)

As specified in the project specification Spraying shall only be done at the minimum temperature when, in the opinion of the Engineer, the road surface temperature is rising. Whenever, in the opinion of the Engineer, the road surface temperature is likely to fall below the minimum temperatures specified, before the commencement of spraying, no spraying shall be carried out.

No bituminous work shall be done during foggy or rainy weather and when a cold wind is blowing the specified temperatures shall be increased by 3O C to 6O C as directed by the Engineer.

Conventional slurry shall not be applied at an air temperature of less than 7O C when temperatures are rising or less than 13OC when temperatures are ropping.

Rapid setting slurry may, if so designed, be laid in air temperatures of 4O C to 40OC and in damp conditions.

During hot weather slurry operations shall be suspended when the spreader box or squeegees are displacing aggregate.

When strong winds are blowing and this is likely to interfere with the proper execution of the work, no surfacing, especially spraying of binder, shall be done.

When the breaking process is so accelerated as to render the product unworkable, eg. By high ambient temperatures, or as otherwise prescribed by the Engineer, no surfacing work shall be done.

(c) Moisture Content

No surface treatment shall be placed unless the moisture content of the upper 50 mm of the road base is less than 50% of the optimum moisture content of the roadbase as determined by the Engineer. To prevent the trapping of water in the pavement structure, after prolonged or intense rain no seal or reseal shall be placed on an existing partly cracked and/or highly permeable surfacing for a period of at least 24 hours or such extended period as determined by the Engineer.

(d) Curing Periods

Unless otherwise indicated in the project specification, the following curing periods shall

apply to the various treatments listed prior to applying a seal or reseal:

Texturing using fine slurry................................................6 weeks

Rapid setting slurry .........................................................12 weeks

Crack sealing .....................................................................2 weeks

Repair of distressed patches..............................................6 weeks

(e) Spraying to cease at 15:00 hours

Unless otherwise agreed by the Engineer, and subject to the satisfactory outcome of a trial section, the Contractor shall programme all spraying operations to cease at 15:00 hours local time each working day.

(f) Trial Areas

Prior to the commencement of normal working the Contractor shall construct a trial area of not less than 1000 square metres using the materials and equipment proposed for the work to demonstrate compliance with the requirements of this Clause.

6.22) CUTTING BACK OF BITUMEN

The cutting back of bitumen will only be allowed where authorised by the Engineer and in accordance with Engineer’s requirements. Only approved kerosene shall be used for cutting back.

The temperature of the bitumen, when the kerosene is introduced, shall not be higher than 140O C.

When cutting back is done in a bitumen distributor, the kerosene shall not be introduced into the distributor through the inspection manhole, which shall be kept closed. The kerosene shall be sucked from 200 liter drums in measured quantities through the bitumen pump and circulated with the bitumen for a minimum of 45 minutes. During this process all burners shall be shut off and no open flames shall be allowed near the distributor.

The following maximum amounts of kerosene shall be added to the basic 150/200 penetration-grade bitumen depending on the road surface temperature at the time of spraying. Lesser amounts than those indicated may be used if conditions on Site allow the development of sufficient adhesion between binder, chippings and existing surface.

Table/14 Addion of kerosene

| Range of surface temperatures(oc) | Approximate corresponding range of ambient air temperatures OC | Maximum addition of Kerosene by volume % |
| --- | --- | --- |
| 16-24 | 10-16 | 7 |
| 24-32 | 16-21 | 5 |
| 32-40 | 21-26 | 3 |
| 40-48 | 26-31 | 1 |
| >48 | >31 | 0 |

6.22.1) HEATING OF BITUMINOUS BINDERS

(a) Conventional Binders

The temperature ranges between which bituminous binders are to be heated shall be as

given in Table /15.

Table /15 Storage and spraying temperature for bituminous binders

| Materials | Maximum storage temperature OC | Heating and spraying temperature OC |
| --- | --- | --- |
|  | <24hours | >24hours | Minimum | Maximum | Recommended |
| Penetration-grade bitumen |
| 60/70 | 175 | 125 | 170 | 190 | 180 |
| 80/100 | 175 | 125 | 165 | 190 | 175 |
| 150-200 | 165125 | 155 | 159 | 175 | 165 |
| Cut-back bitumen |
| RC-250 | 90 | 60 | 90 | 115 | 100 |
| MC-800 | 125 | 75 | 110 | 135 | 125 |
| MC-3000 | 125 | 100 | 135 | 155 | 145 |
| Bitumen emulsions |
| 60% | 60 | Ambient | Ambient | 60 | 60 |
| 65% | 60 | Ambient | 50 | 60 | 60 |
| 70% | 60 | Ambient | 55 | 65 | 65 |

Binders stored in a heated condition shall be kept in a container having a properly

functioning circulatory system and a securely fitting lid. The container shall have a properly functioning built-in thermometer.

Binders that have been heated above the maximum temperatures indicated in Table

/15 shall not be used and shall be removed from Site. During spraying, every effort

shall be made to maintain the binder temperature within 5o C of the recommended spraying temperature.

For surface treatment works the spraying temperature limits for 80/100 penetration-grade

bitumen, cut back with the indicated amounts of kerosene in parts per 100 parts of bitumen by volume as described in Clause shall be as given in Table /16

Table /16 Spaying temperature limits for bituminous binders

| Quantity of Kerosene added (parts per 100 parts bitumen by volume) | Spraying temperature limits OC |
| --- | --- |
|  | Minimum | Maximum | Recommended |
| 0.0 | 150 | 175 | 165 |
| 2.5 | 146 | 163 | 154 |
| 5.0 | 138 | 154 | 146 |
| 7.5 | 132 | 149 | 140 |
| 10.0 | 125 | 143 | 134 |
| 12.5 | 121 | 138 | 129 |
| 15.0 | 115 | 135 | 125 |
| 17.5 | 107 | 127 | 117 |
| 22.5 | 100 | 118 | 108 |

(b) Non-homogeneous (heterogeneous) modified binders (summer grade)

After completion of the bitumen-rubber reaction, the binder shall be cooled to less than

160O C. The binder mixture shall be stored in a container having a properly functioning

circulatory system and a securely fitting lid. The container shall have a properly functioning built-in thermometer. The binder mixture shall not be kept for more than 48 hours before use.

1) The spray and storage conditions of the bitumen-rubber binder shall be in

accordance with the following requirements:

2) Spray temperature: As provided by the supplier

3) Maximum storage time at spray temperature: 4 hours

4) Maximum storage temperature (<48 hours): 35O C less than the spray temperature but not more than 160OC

5) Stored binder heated to a temperature above 160O C shall not be used and

3.23) SINGLE SURFACE TREATMENTS

1 SCOPE

This division covers all the work in connection with the construction of single bituminous

surface treatments for new road construction and for resealing of existing roads.

Note:

The provisions of  Division  "Surface Treatments: Materials and General

Requirements" apply equally to the work covered by this division and will not necessarily

be repeated or specifically referred to in this division.

2 MATERIALS

The materials shall comply with the requirements

The average least dimension (ALD) of the chippings shall comply with the requirements in Table /1.

Table /1 Chippings - Average Least Dimension

| Nominal size (mm) | Minimum ALD(mm) |
| --- | --- |
| 19.0 | 12.0 |
| 13.2 | 8.2 |
| 9.5 | 5.9 |

3.24) DOUBLE SURFACE TREATMENTS

1 SCOPE

This Division covers the supplying and furnishing of materials for the construction of

double bituminous surface treatments.

The double surface treatments shall be constructed using either:

(a) 19.0 mm and 9.5 mm or 6.7 mm chippings, or

(b) 13.2 mm and 6.7 mm or 4.75 mm chippings, as shown in the Bill of Quantities.

Note:

The provisions of Surface Treatments: Materials and General

Requirements", apply equally to the work covered by this division and will not necessarily be repeated or specifically referred to in this division.

2 MATERIALS

The materials shall comply with the requirements given in material section.

The average least dimension (ALD) of the first layer of chippings shall comply with the requirements in Table /1.

Table/1 Chippings - Average Least Dimension

| Nominal Size (mm) | Minimum ALD (mm) |
| --- | --- |
| 19.0 | 12.0 |
| 13.2 | 8.2 |
| 9.5 | 5.9 |

The maximum ALD of the second layer of chippings shall be not more than 50% of the

ALD of the respective first layer

Table /2 Nominal Rates of Application for the First Layer

| Nominal Chipping Size (mm) | Nominal rates of application |
| --- | --- |
|  | Chippings (m3/m2) | Conventional Binder (l/m2) * |
| 9.5 | 0.006 | 0.9 | 1.0 |
| 6.7 | 0.005 | 0.8 | 0.8 |
| 4.75 | 0.004 | 0.6 | 0.6 |

Note: * net cold bitumen; # at spray temperature

Table /3 Nominal Rates of Application for the Second Layer

| Nominal Chipping Size(mm) | Nominal rates of application |
| --- | --- |
|  | Chippings (m3/m2) | Conventional Binder (l/m2) * |
| 9.5 | 0.006 | 1.0 |
| 6.7 | 0.005 | 0.8 |
| 4.75 | 0.004 | 0.6 |

Note: * net cold bitumen

The second application of binder shall preferably take place within 48 hours after the

application of the first layer when penetration-grade bitumen is used for the first layer and not less than ten (10) days after the application of the first layer when cut-back bitumen is used in the first layer.

3.25) TRIPLE SEAL SURFACE TREATMENT

1 SCOPE

This Division covers the supplying and furnishing of materials for the construction of triple bituminous surface treatments.

The double surface treatments shall be constructed using either:

26.5 mm, 13.2 mm and 6.7 mm chippings, or

19.0 mm, 9.5 mm and 6.7 mm chippings, as shown in the Bill of Quantities.

.

2 MATERIALS

The materials shall comply with the requirements of Division material requirement.

The average least dimension (ALD) of the first layer of chippings shall comply with the

requirements in Table /1.

Table/1 Chippings - Average Least Dimension

| Nominal Chipping Size(mm) | Minimum ALD(mm) |
| --- | --- |
| 26.5 | 16.5 |
| 19.0 | 12.0 |

The maximum ALD of the subsequent layers of chippings shall be not more than 50% of the ALD of the respective preceding layers.

3.26)BITUMINOUS ROAD BASES AND

SURFACINGS

1 SCOPE

This section covers all work in connection with the construction of asphaltic bases and

surfacings. It includes the procuring and furnishing of aggregate and bituminous binder,

mixing at a central mixing plant, spreading and compaction of the mixture, as specified for the construction of:

(i) Continuously graded asphalt base;

(ii) Semi-gap-graded asphalt base;

(iii) Continuously graded asphalt surfacing with or without rolled-in pre-coated

chippings:

(iv) Gap-graded asphalt surfacing with or without rolled-in pre-coated

chippings;

(v) Semi-gap-graded asphalt surfacing with or without rolled-in pre-coated

chippings:

(vi) Open-graded asphalt surfacing;

(vii) Stone-mastic asphalt surfacing

The widening of asphalt bases and surfacing, placing asphalt in restricted areas and placing asphalt reinforcing where specified.

The recycling of asphalt by reprocessing recovered materials, adding fresh aggregate, bituminous binders and other agents for obtaining an asphalt mix which will comply with the specified requirements, and placing the recycled material.

The construction of asphalt surfacing on bridge decks where shown on the drawings or ordered by the engineer.

2 MATERIALS

(a) General

All materials shall be handled and stockpiled in a manner that will prevent contamination, segregation or damage. Cement and lime shall be used in the order in which it has been received.

The contractor shall. as often as necessary, test and control the materials produced by himself or the materials received by him from suppliers to ensure that the materials always comply with the specified requirements.

(b) Bituminous binders

The type and grade of bituminous binder to be used in each case shall be as specified hereinafter or in the project specifications.

(i) Conventional binders

The various conventional bituminous binders specified shall comply with the requirements of sub-clause 63A02 (a) (1).

(ii) Non-homogeneous (heterogeneous) modified binders

(The addition of rubber to the aggregate in a similar manner as the addition of filler, the socalled dry method, is not included in these specifications.)

The bitumen-rubber binder shall comply with the following specifications:

(1) Base bitumen

The bituminous binder used in the production of the bitumen-rubber shall be 60/70 or 80/100 penetration-grade bitumen or a blend of these grades to provide a product with a particular viscosity and other prescribed properties.

(2) Rubber

Table/1 Rubber Crumbs

| Sieve Analysis | Test Method |
| --- | --- |
| Sieve Size (mm) | % passing by mass |  |
| 1.18 | 100 | Sabita, BR6T |
| 0.60 | 50-70 |  |
| 0.075 | 0-5 |  |
| Other Requirements |  |
| Natural rubber hydrocarbon content | 30% (minimum) | BS 903, Parts B11 & B12 |
| Resilience (raw) | 40% (minimum | Sabita, BR7T |
| Loss in resilience | 60% (maximum) | Sabita, BR7T |
| Relative density (g/cm3) | 1.10 – 1.25 | Sabita, BR9T |

(3) Extender oil

Extender oil shall be a resinous, high flash point aromatic hydrocarbon conforming with the requirements in table /2.

The chemical composition of the base bitumen and the nature of the rubber will dictate the need to introduce an extender oil. The bitumen and extender oil, when combined shall form a material that is chemically compatible with the rubber.

Table /2 Extender Oils

| Property | Requirements | Test Method |
| --- | --- | --- |
| Flash Point | 180O C (minimum) | ASTM D92 |
| Viscosity at 40O C | 2,500 (minimum) | ASTM D88 |
| Asphaltenes, content by mass | 0.1 % (maximum) | ASTM D2007 |
| Aromatics, content by mass | 55.0 % (minimum) | ASTM D2007 |

Table /3 Bitumen- Rubber Blend

| Property | Requirements |
| --- | --- |
| Rubber content of the total blend by mass | 18 - 24% |
| Extender oil content of the total blend by mass | 4% (maximum) |
| Blending/reaction temperature | 180 – 210 O C |
| Reaction time | 1-4 hours |

A continuous record shall be kept on the site by the contractor of the percentage rubber in the mix and the reaction temperatures and times. The bitumen-rubber binder shall be sampled not more than five minutes prior to the mixing of the asphaltic mix and shall comply with the requirements in table /4.

Table /4 Bitumen- Rubber Binder

| Property | Requirements | Test Method |
| --- | --- | --- |
| Compression recovery: after 5 minutes after 1 hour after 4 hours | 80 - 100% 70 - 95% 25 - 55% | Sabita, BR3T |
| Ring-and-ball softening point | 55 – 62 OC | ASTM D 36 |
| Resilience (%) | 13 - 35% | Sabita, BR2T |
| Dynamic viscosity (Haake at 190O C) | 20 – 50 dPa.s | Sabita BR5T |
| Flow | 15 – 55 mm | Sabita, BR4T |

The bitumen-rubber mixture after reaching the desired consistency shall not be held at temperatures in excess of 160°C (with no extender oil) or 190°C (with 4% extender oil) for more than 4 hours.

(iii) Homogeneous modified binders

Homogeneous modified binders are defined as industrial blends of polymer and bitumen where the blended components form a stable microscopic dispersion, or either or both form a stable continuous phase relative to each other. The properties of the homogeneous modified binders shall comply with the requirements given in the project specifications.

(c) Aggregates

Coarse and fine aggregate shall be clean and free from decomposed materials, vegetable matter and other deleterious substances and shall meet the requirements

(i) Resistance to crushing

The aggregate crushing value (ACV) of the coarse aggregate, when determined in accordance with BS 812-110, shall not exceed the following values for aggregate used for:

Open-graded surfacing........................................................................................................21%

Stone-mastic asphalt     ................................................................................. 21%

Rolled-in chippings.........................................................................................21%

Continuously graded surfacing........................................................................25%

Road bases and leveling courses.......................................................................29%

The minimum dry 10% FACT values of the -13.2 mm + 9.5 mm fraction shall be as follows:

Open-graded surfacing................................................................................ 210 kN

Stone-mastic asphalt....................................................................................210 kN

Rolled-in chippings............................................................................………210 kN

Continuously graded surfacing ................................................................... 160 kN

Roadbases and levelling courses................................................................ 160 kN

The wet/dry ratio shall not be less than 75%.

(ii) Shape of the aggregate

Road base:

The flakiness index when determined in accordance with BS 812-105.1 shall not exceed 35 for the minus 26.5 mm sieve plus 19.00 mm sieve and minus 19 mm plus 13.2 mm sieve fractions respectively.

In addition, at least 50% by mass of the individual fractions retained on each of the standard sieves with a square mesh size of 4.75 mm and larger shall have at least one fractured face.

Surfacing and rolled-in-chippings:

The flakiness index for asphaltic surfacing and rolled-in-chippings shall not exceed the values given in table /5. The grades refer to the single-sized crushed stone grades as defined in sub-clause 6302(b).

Table /5 Flakiness Index

| Nominal Size (mm) | Maximum Flakiness Index% |
| --- | --- |
|  | Asphaltic Surfacing Aggregates | Rolled-in Chippings |
|  | Grade 1 | Grades 2 | All Grades |
| 19.0 | 25 | 30 | 20 |
| 13.2 | 25 | 30 | 20 |
| 9.5 | 30 | 35 |  |
| 6.7 | 30 | 35 |  |

In addition, at least 95% of all particles shall have at least three fractured faces.

(iii) Polishing

The polished stone value (PSV) of aggregates shall not be less than the following values when used for:

PSV

Continuously and open-graded asphaltic surfacing ......50

Stone-mastic asphaltic surfacing...................................50

Gap-graded asphaltic surfacing.....................................45

Rolled-in chippings .......................................................50

Aggregates with PSVs below those stated above may be approved for use by the Engineer.

(iv) Adhesion

When tested in accordance with TMH1 method C5, the immersion index of a mixture of the binder and aggregate proposed for use shall not be less than 75%. The aggregate used for the test mixture shall have a grading within the actual limits for the mix concerned.

(v) Absorption

When tested in accordance with BS 812-105.2, the water absorption of the coarse aggregate shall not exceed 1 % by mass, and that of the fine aggregate shall not exceed 1.5% by mass, unless otherwise permitted.

(vi) Sand equivalent

The total fine aggregate used in all asphalt mixes shall have a sand equivalent of at least 50, when tested in accordance with TMH1 method B19, and the natural sand where it is

permitted to be mixed with the aggregate shall have a sand equivalent of at least 30.

Table /6 grading limits for combined aggregate and mix proportions for asphaltic

Road base

| Type | Semi-gap graded | Continuously graded |
| --- | --- | --- |
| Nominal size | 37.5 mm | 26.5 mm | 37.5 mm | 26.5 mm |
| Sieve size (mm) | Fraction passing by mass (%) |
| 37.5 | 100 |  | 100 |  |
| 26.5 | 85-100 | 100 | 84-94 | 100 |
| 19.0 | 75-95 | 92-100 | 71-84 | 85-95 |
| 13.2 |  | 82-93 | 59-75 | 71-84 |
| 9.5 | 60-80 | 72-87 | 50-67 | 62-78 |
| 6.7 |  | 60-75 |  |  |
| 4.75 | 45-60 | 50-64 | 36-53 | 42-60 |
| 2.36 | 40-52 | 40-52 | 25-42 | 30-47 |
| 1.18 | 36-47 | 36-47 | 18-33 | 21-37 |
| 0.60 | 32-42 | 32-42 |  | 15-30 |
| 0.30 | 22-35 | 22-35 | 9-21 | 11-24 |
| 0.15 | 10-20 | 10-20 | 6-17 | 8-19 |
| 0.075 | 4-10 | 4-10 | 4-12 | 5-12 |
| Nominal mix proportions by mass (%) |
| Aggregate | 93.5 | 93.5 | 95.0 | 94.5 |
| Bitumen | 5.5 | 5.5 | 4.0 | 4.5 |
| Active filler | 1.0 | 1.0 | 1.0 | 1.0 |
| Total | 100.0 | 100.0 | 100.0 | 100.0 |

* For tender purposes only Active filler shall be hydrated lime.

Table/7 Grading limits for combined aggregate and mix proportions for asphaltic

Surfacing

| Type | Gap-graded | Semi-gap-graded |
| --- | --- | --- |
| Stone Content | High | Intermediate | Low | - | - |
| Nominal size | - | - | - | 26.5 mm | 19.0 mm |
| Sieve size (mm) | Fraction passing by mass (%) |
| 26.5 | - | - | - | 100 | - |
| 19.0 | 100 | 100 | 100 | 92-100 | 100 |
| 13.2 | 75-100 | 75-100 | 75-100 | 82-93 | 82-100 |
| 9.5 | 65-85 | 70-90 | 70-90 | 72-87 | 73-86 |
| 4.75 | 50-60 | 60-70 | 65-75 | 50-64 | 45-60 |
| 2.36 | 45-55 | 53-63 | 60-70 | 40-52 | 40-52 |
| 1.18 | 45-55 | 53-63 | 60-70 | 36-47 | 36-47 |
| 0.60 | 36-52 | 45-63 | 55-70 | 32-42 | 32-42 |
| 0.30 | 25-45 | 35-55 | 45-65 | 22-35 | 22-35 |
| 0.15 | 12-32 | 15-35 | 20-40 | 10-20 | 10-20 |
| 0.075 | 5-12 | 5-12 | 5-12 | 4-10 | 4-10 |
| Nominal mix proportions by mass (%) |
| Aggregate | 92.0 | 92.0 | 92.0 | 93.0 | 93.0 |
| Bitumen | 7.0 | 7.0 | 7.0 | 6.0 | 6.0 |
| Active filler | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 |
| Total | 100.0 | 100.0 | 100.0 | 100.0 | 100.0 |

* The percentage passing the 4.75 mm sieve and retained on the 0.600 mm sieve shall not exceed 15%

Table /8 Grading limits for combined aggregate and mix proportions for asphaltic

surfacing

| Type | Continuously-graded | Semi-open Graded |
| --- | --- | --- |
| Grading | Coarse | Medium | Fine |  |
| Sieve size (mm) | Fraction passing by mass (%) |
| 26.5 | 100 | - | - | - |
| 19.0 | 85-100 | - | - | 100 |
| 13.2 | 71-84 | 100 | - | 70-100 |
| 9.5 | 62-76 | 82-100 | 100 | 50-82 |
| 4.75 | 42-60 | 54-75 | 64-88 | 16-38 |
| 2.36 | 30-48 | 35-50 | 45-60 | 8-22 |
| 1.18 | 22-38 | 27-42 | 35-54 | 4-15 |
| 0.60 | 16-28 | 18-32 | 24-40 | 3-10 |
| 0.30 | 12-20 | 11-23 | 16-28 | 3-8 |
| 0.15 | 8-15 | 7-16 | 10-20 | 2-6 |
| 0.075 | 4-10 | 4-10 | 4-12 | 1-4 |
| Nominal mix proportions by mass (%) |
| Aggregate | 93.5 | 93.5 | 93.0 | 90.5 |
| Bitumen | 5.5 | 5.5 | 6 | 8.5 |
| Active filler | 1.0 | 1.0 | 1.0 | 1.0 |
| Total | 100.0 | 100.0 | 100.0 | 100.0 |

* Dry method rubberised asphalt as specified in the project specifications.

Table /9 Grading limits for combined aggregate and mix proportions for

continuously graded asphaltic surfacing using non-homogeneous modified

bituminous binders

| Nominal size | 19.0 mm | 13.2 mm |
| --- | --- | --- |
| Sieve size (mm) | Fraction passing by mass (%) |
| 19.0 | 100 | - |
| 13.2 | 84-96 | 100 |
| 9.5 | 70-84 | 80-100 |
| 4.75 | 45-63 | 50-70 |
| 2.36 | 29-47 | 32-50 |
| 1.18 | 19-33 |  |
| 0.60 | 13-25 | 13-25 |
| 0.30 | 10-18 | 8-18 |
| 0.15 | 6-13 |  |
| 0.075 | 4-10 | 4-8 |
| Nominal mix proportions by mass (%) |
| Aggregate | 91.0 | 91.0 |
| Modified binder (bitumen rubber) | 7.0 | 7.0 |
| Active filler | 2.0 | 2.0 |
| Total | 100.0 | 100.0 |

Table /10 Grading limits for combined aggregate and mix proportions for open

graded asphaltic surfacing using conventional, non-homogeneous modified

and homogeneous modified bituminous binders

The selected target grading for open-graded asphalt mixes shall be such that in the case of

medium open-graded asphalt mixes of type 2 and 3, the void content of the compacted mix shall be between 18% and 22%, while for all other types, the void-content shall be between 20% and 25%.

| Nominal size | 13.2mm | 9.5mm |
| --- | --- | --- |
| Type | Type 1 | Type 2 | Type 3 |  |
| Sieve size (mm) | Fraction passing by mass (%) |
| 19.0 | 100 | 100 | 100 | 100 | - | - |
| 13.2 | 90-100 | 90-100 | 90-100 | 70-100 | 100 | - |
| 9.5 | 30-50 | 30-50 | 30-50 | 50-80 | 50-70 | 100 |
| 4.75 | 10-20 | 10-20 | 10-20 | 15-30 | 20-30 | 10-25 |
| 2.36 | 8-14 | 8-14 | 8-14 | 10-22 | 5-15 | 5-15 |
| 1.18 | - | - | - | - | - | - |
| 0.60 | - | - | - | 6-13 | - | - |
| 0.30 | - | - | - | - | 3-8 | - |
| 0.15 | - | - | - | - | - | - |
| 0.075 | 2-6 | 2-6 | 2-6 | 3-6 | 2-5 | 2-6 |
| Nominal mix proportions by mass (%) |
| Binder type | Penetration Grade | Polymer Modified | Bitumen- Rubber | Bitumen- Rubber | Bitumen- Rubber | As for type 1 |
| Aggregate | 94.5 | 94.0 | 93.5 | 93.5 | 93.5 | As for type 1 |
| Bitumen | 5.0 | 5.0 | 5.5 | 5.5 | 5.5 | As for type 1 |
| Active filler | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 |
| Total | 100.0 | 100.0 | 100.0 | 100.0 | 100.0 | 100.0 |

Table /11 Grading limits for combined aggregate and mix proportions for stone

mastic asphaltic surfacing using conventional and homogeneous modified

bituminous binders

| Aggregate size | 13.2mm | 9.5mm | 6.7mm |
| --- | --- | --- | --- |
| Sieve size (mm) | Fraction passing by mass (%) |
| 13.2 | 100 | - | - |
| 9.5 | 67-90 | 100 | - |
| 6.7 | 41-65 | 50-80 | 100 |
| 4.75 | 30-50 | 30-55 | 80-100 |
| 2.36 | 21-32 | 22-32 | 34-44 |
| 1.18 | 17-27 | 17-27 | 24-34 |
| 0.60 | 14-24 | 14-23 | 18-30 |
| 0.30 | 11-23 | 11-22 | 13-25 |
| 0.15 | 9-17 | 9-19 | 9-19 |
| 0.075 | 7-12 | 7-12 | 7-12 |
| Nominal mix proportions by mass (%) |
| Aggregate | 93.0 | 93.0 | 93.0 |
| Binder | 6.5 | 6.5 | 6.5 |
| Binder stabiliser (cellulose fibres) | 0.5 | 0.5 | 0.5 |
| Total | 100.0 | 100.0 | 100.0 |

(ix) Additional requirements for asphaltic roadbases

Unless otherwise specified in the project specifications, if approved by the engineer, the

aggregate component may contain not more than 10% by mass of natural fines not obtained

from the parent rock being crushed. The added fines shall have a liquid limit not more than 25% and a PI not more than 6. The contractor shall submit full details regarding the exact quantity and nature of such fine aggregate, before such permission will be considered. In the event of such added material being natural sand, its impact on dynamic creep properties should be assessed from laboratory briquettes and cores obtained in a trial section completed well in advance of any production runs. The natural fines shall be added to the mix from a dedicated cold feed bin.

(x) Rolled-in chippings

Rolled-in chippings for asphalt surfacing mixes shall comply with the grading requirements

of table /12.

Table /12 Grading limits for rolled-in chippings

| Nominal size | 19.0mm | 13.2mm |
| --- | --- | --- |
| Sieve size (mm) | Fraction passing by mass (%) |
| 19.0 | 100 | - |
| 13.2 | 0-20 | 100 |
| 6.7 | 0-5 | 0-20 |
| 0.425 | 0-1 | 0-5 |
|  | 0-0.5 | 0-0.5 |

(d) Fillers

If the grading of the combined aggregates for asphalt surfacing mixes shows a deficiency in fines, an approved filler may be used to improve the grading. Filler may consist of active filler as defined hereinafter or of inert material such as rock dust having the required grading necessary to improve the grading of the combined aggregates. In no instance shall more than 2% by mass of active filler be used in asphalt mixes. Inert filler such as rock dust used to improve grading shall not be subject to this limitation.

The engineer may order the use of any active filler to improve the adhesion properties of the aggregate. Active filler shall consist of milled blast furnace slag, hydrated lime, ordinary portland cement, portland blast furnace cement, fly-ash, or a mixture of any of the above materials. Individual materials shall comply with the requirements of the relevant specifications for such material. Active filler shall have at least 70% by mass passing the 0.075 mm sieve and a bulk density in toluene between 0.5 and 0.9 g/m l. The voids in dry compacted filler shall be between 0.3% and 0.5% when tested in accordance with BS 812.

Active fillers for use in asphalt bases shall be introduced to the mix prior to wetting with the binder. An active filler content of 1.0% by mass shall be used unless otherwise specified.

Only active filler added on the instructions of the engineer, for the purpose of improving

adhesion, will be paid for. No payment will be made for filler added to improve the grading.

(e) Fibres

The use of fibres in asphalt mixes shall be subject to the provisions of the project

specifications.

(f) Asphalt reinforcing

Asphalt reinforcing shall be of the type specified in the project specifications and shall be

obtained from an approved manufacturer.

Where the use of reinforcing for asphalt has been specified, at least 3 months before the

material is to be used the contractor shall submit to the engineer for approval samples of the type he intends to use, together with complete specifications of the material and the

manufacturer's instructions for use. Where the material does not carry the verification mark of an approved authority, the engineer may instruct the contractor to have the material tested by an approved laboratory and to submit the results.

(g) Asphaltic materials for hot plant mix recycling

(i) Recovered asphaltic mixes

The engineer will test the existing asphaltic materials in any part of the project and determine its suitability for recycling before removal. He may instruct the contractor to drill additional cores at specified points. Recovered asphalt intended for recycling shall be stored separately from other asphalt, and the engineer may also direct different types of asphalt to be stored separately.

The recovered asphalt shall be free from any underlying base material and other foreign matter.

Asphalt milled out shall be of a maximum size of 37.5 mm, unless otherwise approved by the engineer.

Asphalt not milled out shall be broken down in any approved manner so that it can be properly remixed in a plant to the satisfaction of the engineer. Mixes of recycled asphalt containing fragments of recovered asphalt exceeding 37.5 mm in size, will not be accepted.

Payment for recovered asphalt will distinguish between milled out and non-rnilled out material.

Samples shall be taken from the recovered asphalt intended for hot recycled mixes in the stockpile and shall be tested for grading and quality of the aggregate, binder content, and properties of the binder.

(ii) Bituminous binders

The provisions of sub-clause 6402(b) shall apply.

The grade of new binder used in the recycled asphalt mix shall be such that the mix of new and residual binder will comply with the requirements of the project specifications.

Recycling agents such as blended oils and other additives may not be used without prior approval by the engineer.

(iii) New aggregate

New aggregate required for use in recycled asphalt mixtures shall comply with the requirements

(iv) Combined aggregate

The aggregate mix obtained from new aggregate and the aggregate in the recovered asphalt, including any mineral filler, an approved quantity of which may be added in accordance with sub-clause 6402(d), shall comply with the requirements specified in the project specifications for the relevant recycled asphalt layer.

(v) Storing material for recycling

The provisions of clause5306 shall apply to the storing of recovered asphalt.

In addition the following requirements shall apply:

(1) Stockpiles of milled or crushed asphalt shall be shaped and formed in a manner that will prevent segregation as far as possible. The stockpiling of the recovered asphalt shall be done in a manner that will prevent consolidation as far as possible, and adequate covers shall be provided to prevent the ingress of water and contamination by dust.

(2) The recovered asphalt that is placed in the stockpile(s) shall be tested, carefully controlled and recorded with regard to origin and material properties to ensure a consistent recycled end product.

(3) The preparation of stockpile sites and the stockpiling of recovered asphalt for

recycling will not be paid for directly but full compensation therefore shall be included in the rates for the recycled asphalt.

(h) Hot in situ surface recycling

Hot in situ surface recycling shall comply with the requirements in the project specifications with regard to new binder, recycling additives, new asphaltic mixes, new aggregate or combinations of these materials.

Table/13 Design requirements for asphaltic mixes Road base

|  | Roadbase(37.5mm aggregate) | Continuously graded and stone mastic wearing courses | Continuously graded bitumen rubberwearing courses | Open-graded asphalt wearing courses |  |
| --- | --- | --- | --- | --- | --- |
| Design guidelines | AASHTO R 12, Sabita M13, TRH 8 | AASHTO R 12, TRH 8 | - | AASHTO R 12, Sabita M16, TRH 8, | AASHTO R 12, TRH 8, - |
| Voids in mix (%) | 3-6 | 3-6 | 2-6 | 9.5mm: 20-25 type1: 20-25 type 2:18-22 type 3:18-22 | 3-6 |
| Voids in mineral aggregate (%) (minimum) | 12 | Continiously graded:14 stone mastic: 17 | 17 | 25 | 26.5mm:14 19.0mm:15 |
| Indirect tensile strength at 25O C (kPa) | 800 | 800 | 550 | - | 800 |
| cantabro abration loss at 25oc(maximum) | - | - | - | 25 (type 2: 20) (type 3: 20) | - |
| Dynamic creep at 40oc c for labratory briquettes (mpa)(minimum) | 15 | 15(for stone mastic see project specification) | 10 | Not applicable | 12 |

6.27) PRE-COATED CHIPPINGS FORASPHALT SURFACING

Aggregate for pre-coated chippings shall be coated using 1.7% +/- 0.3% by mass of the

same bitumen used in the asphaltic surfacing, provided that the bitumen shall not be softer than 60/70 penetration-grade. One per cent by mass of active filler shall be added to the mixture.

The aggregate shall be dried and fed into the mixer at a temperature of between 130° C and 185° C followed by the bitumen (at a temperature not exceeding 175° C) and filler.

Immediately after the aggregate has been coated and discharged from the mixer it shall be

rapidly cooled to ambient air temperature by hosing down with water.

Coated chippings shall be stockpiled in heaps not exceeding 1.0 meter in height and, if

necessary, protected to prevent its temperature from exceeding 60° C during storage.

The pre-coated chippings shall be spread on the asphaltic surfacing at the rate of 6 to 8

kg/m2 when using 13.2 mm nominal size chippings, 7 to 9 kg/m2 when using 19.0 mm

nominal size chippings, depending on the relative density of the aggregate. The chippings

shall be laid by a mechanical spreader, which straddles the paved width and follows

immediately behind the paver.

6.27.1) CONSTRUCTION TOLERANCES

(a) Construction tolerances

The completed sections of asphaltic base and surfacing shall comply with the requirements for grade, width, thickness, cross section and smoothness stated below.

(i) Level and grade

The level tolerances referred to in clauses 10205 and 10305 shall be as follows:

H90 ................................................. + / - 15 mm

Hmax .......................................................................+ / - 20 mm

Deviation from the specified longitudinal grade due to deviations from the specified levels shall not exceed the values given below:

Length of variation in grade Maximum variation from specified grade

(m) (%)

2 ........................................................................................... 0.354

5 ........................................................................................... 0.224

10 ........................................................................................... 0.158

20 ........................................................................................... 0.112

30 ........................................................................................... 0.091

(ii) Width

The average width of both asphalt base and surfacing shall be at least equal to that shown on the drawings and nowhere shall the outer edge of the layer be inside the lines shown on the drawings by more than 15 mm in the case of both asphaltic base and asphaltic surfacing.

(iii) Thickness

The thickness tolerances referred to in clauses 8205 and 8305 shall be as follows:

Base Surfacing

D90............................15 mm.............................................. 5 mm

Dmax..........................20 mm.............................................. 8 mm

Dave.............................5 mm.............................................. 2 mm

Thickness shall be determined from carefully controlled levels taken before and after

construction in exactly the same position and/or from cores drilled from the completed

layer.

(iv) Cross section

When tested with a 3 m straightedge laid at right angles to the road centre line the surface

shall not deviate from the bottom of the straight-edge by more than 6 mm for freeways and by more than 10 mm for other roads.

At any transverse section the difference in level between any two points shall not vary from their difference in level computed from the cross section shown on the drawings by more than 15 mm for freeways and 20 mm for other roads.

(v) Surface regularity

When tested with a rolling straight-edge as described in clause 10111 the number of surface irregularities shall not exceed those given below (applied to base and surfacing)

(1) Average number of irregularities per 100 m equal to or exceeding the specified value when taken over 300 m - 600 m lengths:

Freeways (3 mm irregularities)

Asphaltic mixes with rolled-in chippings .......5

Stone-mastic asphaltic mixes ..........................4

Other asphaltic layers ......................................3

Other roads (5 mm irregularities)

Asphaltic mixes with rolled-in chippings .......4

Other asphaltic layers ......................................2

(2) Number of irregularities equal to or exceeding the specified value when taken over

100 m sections:

Freeways (3 mm irregularities)

Asphaltic mixes with rolled-in chippings .......8

Stone-mastic asphaltic mixes ..........................6

Other asphaltic layers ......................................5

Other roads (5 mm irregularities)

Asphaltic mixes with rolled-in chippings .......6

Other asphaltic layers ......................................3

(3) The maximum value of any individual irregularity when measured with the rolling

straight-edge or a 3 m straight-edge laid parallel to the road centre line:

Freeways

Asphaltic mixes with rolled-in chippings ...... 5 mm

Stone-mastic asphaltic mixes......................... 6 mm

Other asphaltic layers .................................... 4 mm

Other roads

Other roads..................................................... 8 mm

(vi) Multiple-layer base

Where the base is constructed from more than one layer, the requirements specified shall

apply to the combined layers in respect of width and thickness. The requirements for crosssection,

smoothness and grade shall apply to the final layer only but the lower layers shall

be constructed so as to ensure that these requirements in the final layer can be met.

(vii) Surfacing of bridge decks

The completed surfacing shall comply with the requirements for base in respect of surface tolerances for grade, smoothness, cross section and width.

(b) Spread rate of rolled-in chippings

The tolerance in the spread rate of rolled-in chippings shall be + / - 10% of the specified spread rate.

(c) Gradings

The combined aggregate and filler grading shall not deviate from the approved target grading for the working mix by more than that given in table 6400/15. The mean grading of each lot of the working mix (minimum of 6 tests per lot) shall be determined from samples obtained in a stratified random sampling procedure.

Table/15 Deviation from approved target grading

| Material passing sieve size(mm) | Permissible deviation from approved target grading (%) |
| --- | --- |
| 26.5 | ± 5 |
| 19 | ± 5 |
| 13.2 | ± 5 |
| 9.5 | ± 4 |
| 6.7 | ± 4 |
| 4.75 | ± 4 |
| 2.36 | ± 4 |
| 1.18 | ± 4 |
| 0.60 | ± 4 |
| 0.30 | ± 3 |
| 0.15 | ± 2 |
| 0.075 | ± 1 |

* When statistical methods are applied the permissible deviation for the 0.075 mm fraction is + / -2.0%.

.

6.28)BITUMINOUS ROAD-MIX SURFACING

1 SCOPE

This work shall consist of aggregate and bituminous material mixed in place on a prepared surface and constructed in accordance with these Specifications and in conformity with the lines, grades, and typical cross section shown on the Drawings. Aggregate shall consist of either new aggregate (Case 1), or aggregate present in the existing road (Case 2), whichever is called for in the Project Specifications.

The percentage of bituminous material, by weight, to be added to the aggregate will usually be between 3.5 and 7 percent of the weight of the dry aggregate. The exact percentage to be used shall be fixed by the Engineer based on preliminary laboratory tests and field sieve analyses of the aggregates furnished or in place.

2 MATERIALS

(a) New Aggregate (Case 1)

New aggregate (Case 1) shall consist of coarse aggregate of crushed gravel, crushed

boulder, or crushed rock, composed of hard, durable particles and a filler of finely crushed stone, sand, or other finely divided mineral matter. The portion of the material retained on a 5 mm sieve shall be known as coarse aggregate, and that portion passing a 5 mm sieve shall be known as fine aggregate. The total mineral aggregate shall be graded within one of the gradations shown in Table 6900/1, whichever is called for in the Project Specifications, when tested in accordance to AASHO T 11 and T 27.

Table 6900/1 Grading Requirements for Road Mix Bituminous Surface Courses

| Sieve Size(mm) | Percentage passing (by weight) |
| --- | --- |
|  | A | B | C | D |
| 28 | 100 | 100 | - | - |
| 20 | 85-100 | 75-100 | 100 | - |
| 14 | - | - | 40-65 | 100 |
| 5 | 45-65 | 30-60 | 25-50 | 50-70 |
| 2 | 30-50 | 20-50 | 12-40 | 30-50 |
| 0.425 | 10-25 | - | 3-20 | - |
| 0.075 | 3-10 | 3-10 | 0-10 | 3-10 |

If crushed gravel is used, not less than 50 percent by weight of the coarse aggregate particles retained on the 5 mm sieve shall be particles having at least one fractured face.

The coarse aggregate shall have a percentage of wear of not more than 40 at 500 revolutions, as determined byAASHTO T 96. That portion of the aggregate passing a 5 mm sieve shall have a plasticity index of not more than 6, as determined by AASHO T 90 or a liquid limit not greater than 30, as determined by AASHTO T 89.

The fine aggregate shall be in accordance with AASHTO M 29, and the mineral filler in accordance with AASHTO M 17.

The material shall be free from clay balls and adherent films of clay or other matter that would prevent thorough coating with bituminous material.

(b) Aggregate from the Existing Surface (Case 2)

Where aggregate required for the road-mix surface course is already in place, the Contractor shall not be responsible for its grading or quality except for removal of oversize pieces. In general, salvaged aggregate to be used for road-mix surface course will consist of material meeting the requirements given above for new aggregate or may consist of selected granular material of other gradings. Any particles of salvaged aggregate appearing in the surface at the time of lay-down and finishing that will not pass a 37.5 mm sieve shall be removed by the Contractor as directed by the Engineer.

(c) Bituminous Materials

Bituminous materials shall be of the type and grade called for in the Project Specifications.